Internal erosion process and its influence factors in widely graded loose soils due to rainfall infiltration

Li Liang1, Da-Lang Tian2,3, Zheng-chuan Li3

1 Chongqing Jianzhu College, Chongqing 400072, P.R.China

2School of Civil Engineering, Chongqing Unversity, Chongqing 400045, P.R.China

3Chongqing Survey, Design and Research Institute Co., Ltd. Of CREEC, Chongqing 400023, P.R.China

Abstract: Widely graded loose soils (WGLS), a loose mixture comprising coarse and fine particles, are widely distributed in the western mountainous areas of China. Owing to rainfall infiltration, fine particles are eroded and migrated through the skeleton formed by coarse particles, thus altering the hydraulic and mechanical characteristics of WGLS. This paper intends to uncover the internal erosion process and its influencing factors in WGLS due to rainfall infiltration. To this end, a novel fixed-wall permeameter is developed, capable of applying an inflow rate-controlled condition and collecting effluent flowing out of the specimen. A simplified and cost-effective testing protocol is proposed for separating eroded silty clay particles, sandy gravel particles, and seepage water from the collected effluent. Several seepage tests are conducted on remolded specimens with different inflow rates and initial porosity utilizing the newly developed experimental setup and testing protocol. The results indicate four successive erosion stages in the internal erosion process: the suffusion stage, the suffosion stage, the piping stage, and the stabilization stage. Six critical hydraulic gradients correspond to the onset of the various stages. The inflow rate does not affect the critical hydraulic gradient for suffusion. However, it significantly impacts the critical hydraulic gradient for suffosion and subsequent internal erosion behavior. Increasing initial porosity does not necessarily result in higher erosion potential. These results are conducive to further understanding the formation mechanism of internal erosion-induced geologic hazards.

Keywords: Internal erosion; Widely graded loose soils; Fixed-wall permeameter; Soil column seepage test

1 INTRODUCTION

Loosely deposited soils, such as landslide, debris-flow, and artificial deposits, are widely distributed in the western mountainous areas of China due to frequent earthquakes, debris-flow disasters, and engineering construction (Ni et al., 2012; Zhang et al., 2021; Li et al., 2023). Field observation shows that these loosely deposited soils typically have wide-graded particle size distribution with a range of size from clay (particle size < 0.001 mm) to boulder (particle size > 100 mm), unconsolidated and non-uniform pore structures, and are therefore also known as widely graded loose soils (WGLS) (Guo & Cui, 2020). Coarse particles usually form a soil matrix, while fine particles fill the matrix void and can bond to coarse particles (Cui et al., 2019). During rainfall events, the groundwater seepage process leads to the migration of fine particles between the matrix formed by coarse particles, thereby accumulating fine particles at the bottom of the slope (Tian et al., 2020a), as depicted in Fig. 1(a). Such a migration process is commonly referred to as internal erosion induced by water infiltration. Fine migration inevitably alters the porosity of WGLS and influences their physical and mechanical characteristics, which is non-negligible for geotechnical and geological engineering (Tian et al., 2020b; Liang et al., 2020a; Jiang et al., 2023). Furthermore, fines accumulation generally generates a relatively impermeable layer, impeding further downward water infiltration, forming a weak plane in the slope, and influencing the stability of the slope (Crosta & Prisco, 1999, Wang et al., 2016).

Due to the significant impacts mentioned above, internal erosion in WGLS due to rainfall infiltration is increasingly recognized as the leading cause of geologic and geotechnical disasters in fragile mountain areas and valley terrains, such as local collapse, shallow slope failure, and debris flows (Cui et al., 2014; Guo et al., 2016). For example, the slope failure of the Lei-Yi Highway in Southwest China (Yuan & Che, 2022), the landslide of the Tangier-Port Tangier Med and Fez-Taza highway sections in northern and northeastern Morocco through mountainous areas (Chehlafi et al., 2019), and the large debris flow in Wenjia Ravine in the Wenchuan earthquake-affected area (Cui et al., 2017), are recorded as prominent representatives of geological hazards due to internal erosion in WGLS. In addition, internal erosion of soils is a hidden process that may remain undetected at the surface until a collapse occurs, and even in extreme erosion events, the erosion evidence is often washed away after the collapse (Lindow et al., 2009; Gu et al., 2019). Therefore, an in-depth understanding of seeping water erodes in WGLS is important for geotechnical engineering, engineering geology, and geo-hazard phenomenon.

Internal erosion is a coupled process that involves fines detachment from the pore surface between the soil matrix, fines transport as suspension, and possible fines redeposition at the pore surface or pore throats, as shown in Fig. 1b (Kenney & Lau, 1985; Khilar & Fogler, 1998). Internal erosion takes different forms depending on the stress state and subsequent fate of the transported fine grains. Generally, three phenomena responsible for internal erosion in granular materials are suffusion, suffosion, and piping (Richard & Reddy, 2007; Moffat et al., 2011; Fannin & Slangen, 2014). In suffusion, the stress-free finer fraction moves within the coarser fraction without disturbing the structure of the coarser fraction. It features a mass loss, no change in volume, and a subtle increase in hydraulic conductivity. In suffosion, the movement of fine particles, which partially constitute force-chain contacts, is accompanied by the destruction of the soil structure. It manifests as a significant mass loss, large and rapid changes in hydraulic conductivity, and a potential for the collapse of the soil matrix. Piping refers to the phenomenon in which underground water flows along continuous openings, such as cracks, and fine grains on the wall of the openings are mobilized and washed out of the matrix by concentrated seepage, resulting in a tubular channel or pipe. These qualitative distinctions between the three phenomena are used herein to describe the temporal progression of internal erosion in WGLS.

(a)                             (b)

FIGURE 1 Schematic illustration of the fines migration process in WGLS due to rainfall infiltration: (a) fines migration and accumulation in an infinite slope; (2) coupled process of internal erosion in WGLS

Extensive field inspections, laboratory testing, and numerical simulation studies have been conducted to mitigate internal erosion risk. Some studies have focused on the mechanism and process of internal erosion (Wan & Fell, 2008; Bendahmane et al., 2008), and they concluded that the following two conditions must be met for internal erosion to occur: (1) the size of fines must be smaller than the size of the constrictions between the coarser particles; (2) the action of hydraulic flow must be sufficient to detach the fine particles. The first condition is associated with the intrinsic properties of soil. Therefore, some researchers have established correlations between soil parameters, including fines content (Li et al., 2020), fabric (Shire et al., 2014), relative density (To et al., 2020), grain morphology (Maroof et al., 2021), and internal erosion characteristics, to shed light on the intrinsic factors affecting the seepage failures in soil. The second condition is related to hydro-mechanical condition applied to fine particles, which depends on external factors. Thus, external factors affecting the internal erosion of soil, such as stress states (Ma et al., 2021), flow direction (Liang et al., 2020b), and hydraulic loading history (Rochim et al., 2017), have also been extensively studied. After understanding the mechanisms of internal erosion and its influencing factors, various criteria have been proposed based on the geo-hydro-mechanical characteristics, such as particle size distribution (To et al., 2018; Chapuis & Saucier, 2020), stress reduction factor (Skempton & Brogan, 1994; Li & Fannin, 2012), critical hydraulic shear stress (Reddi et al., 2000), critical hydraulic gradient (Israr & Indraratna, 2019), and power dissipated flow (Martot et al., 2011) to assess the susceptibility of soil mass to internal erosion. Recognizing the significant impact of internal erosion on soil structure, many scholars have gradually started researching the influence of internal erosion on soil mechanics behavior (Taha et al., 2022; Liang et al., 2023).

Previous studies have mainly focused on the internal erosion of gravelly soils in artificial structures with a relatively constant hydraulic loading over a long period, such as dams and dikes, while there has been less research on the internal erosion of WGLS related to slope stability under rainfall infiltration. In the latter, hydraulic loading applied on soils undergo rapid and significant changes within a short period. For the internal erosion of WGLS, soil column infiltration, laboratory flume, and in situ artificial rainfall experiments are generally the three commonly used test methods (Yin et al. 2019). In terms of laboratory flume tests, Hu et al. (2022) carried out a centrifugal modeling test to study the erosion failure behaviors of soil-rock mixture slopes. Xiao et al. (2022) utilized flume tests to investigate the effects of microbially induced calcite precipitation (MICP) treatment on the erosion resistance of sandy slopes with different uniformity coefficients. As for in situ artificial rainfall experiments, Yuan & Che (2022) performed an in situ rainfall model test on a decomposed granite slope to clarify the evolution process and spatio-temporal characteristics of slope erosion with the help of electrical measurements and laser scanning.

However, these experimental methods are impractical in quantifying the impact of internal erosion on WGLS under rainfall in real-time. Soil column infiltration testing is an effective method to address this issue. Wang et al. (2011) conducted soil column experiments on soil from a debris flow source area in Jiangjiagou ravine to study the influence of particle transport and clogging effects on the permeability of soils. Zhu et al. (2021) conducted soil column permeability tests using a self-made permeameter to study the influence of fabric on the hydraulic conductivity of WGLS while considering the fines migration. Mao et al. (2022) utilized a self-made apparatus system to analyze the effects of muddy water seepage on the permeability of coarse-grained soil columns. Notably, the hydraulic-gradient controlled conditions are applied in all soil column infiltration tests mentioned above, which differ from the hydraulic conditions experienced by the soil under rainfall infiltration. Furthermore, the temporal progression of internal erosion is also eliminated, which is vital for an in-depth understanding of the internal erosion-induced slope failure.

In this work, we aim to gain a deeper understanding of the internal erosion process of WGLS under rainfall infiltration and reveal its influencing factors. To this end, a fixed-wall permeameter is developed to apply inflow-rate controlled conditions, which is used to simulate rainfall infiltration. A soil-fluid separation testing protocol is proposed to distinguish silty clay and sandy gravel fraction erosion. A series of downward seepage tests on reconstitute specimens under inflow-rate controlled conditions are conducted using the newly developed device and testing protocol. Moreover, different flow rates are applied, and samples with varying porosities are used. The results are discussed in terms of hydraulic gradient, outflow rate, silty clay fraction erosion rate, and sandy gravel fraction erosion rate. Finally, a detailed description of the internal erosion process of WGLS due to rainfall infiltration is provided, and the effects of inflow rate and initial porosity on internal erosion behaviors are studied. The research findings are expected to provide a basis for further investigation into the mechanisms of hydrodynamic-induced landslide and stability analysis of slope deposits.

2 LABORATORY EXPERIMENTS

2.1 Experimental apparatus and soil-fluid separation testing protocol

The fixed-wall permeameter developed by the authors (Tian et al., 2020a) is used in this study. It can perform seepage erosion tests on unconsolidated WGLS specimens with unidirectional downward seepage at a constant inflow rate. Compared to hydraulic-gradient controlled conditions, the constant inflow rate hydraulic loading better represents the actual hydraulic conditions experienced by the soil during rainfall infiltration. In addition, a solid-fluid separation testing protocol is proposed to extract eroded silty clay particles, eroded sandy gravel particles, and permeating fluid from the effluent exiting from the downstream surface of the specimens, by which the erosion rate of the eroded grains, including silty clay particles and sandy gravel particles, and the average hydraulic conductivity can be determined.

2.1.1 Experimental apparatus

The schematic illustration of the testing apparatus is shown in Fig. 2a. It comprises an adjustable frame, a constant flux water supply system, an effluent collection system, and a rigid-wall permeameter cell. This adjustable framework is constructed by linking three light-rounded acrylic plates, i.e., base plate, top plate, and adjustable middle plate, with screws. The positions of the top and base plates are fixed, while the relative position of the middle plate can be adjusted according to the requirements of the experiment. Before the experiment, a leveling instrument is used to check the horizontal level of the intermediate plate to ensure vertical seepage. The water is from the water supply system that includes upper and lower reservoirs placed on the electronic balance, a peristaltic pump with the flux control function, and a standing pipe made of transparent plexiglass. These electronic balances are linked to a data acquisition system for continuously measuring the weight of the upper and lower reservoirs. The peristaltic pump is installed between the upper reservoir and the standing pipe to control the inflow rate of the internal erosion experiment. An overflow pipe is arranged on one side of the standing pipe at 50.0 cm from the top of the sample. When the water level exceeds the height of the overflow pipe, excess seepage water will enter the lower reservoir, which ensures the maximum hydraulic gradient imposed on samples. The effluent collection system is composed of an inverted cone funnel and a series of numbered collection cups. It is designed for the continuous collection of effluent seeping downstream of the specimen at every scheduled time interval.

The rigid-wall permeameter cell shown in Fig. 2(b) is a critical component of the developed experimental apparatus. It is made of transparent acrylic pipe and can accommodate a soil specimen of 39.1 mm in diameter and 80.0 mm in height. A rubber membrane is attached to the inside wall of the permeameter to avoid unexpected parasitic flow between the compacted specimen and the rigid wall of the permeameter, which perplexing the conventional fixed-wall permeameter (Kenney & Lau, 1985; Bendahmane et al., 2008). A layer consisting of 2 mm single-sized glass balls serves to break up the incoming flow to ensure uniform water flow on the upper surface of the tested specimen. A upper perforated plate with an opening size of 1 mm is employed to support the glass balls layer and to eliminate the effect of gravity from glass beads on the internal erosion behavior of the sample. In addition, the nonwoven textile is placed between the upper perforated plate and the top surface of the specimen to prevent upward fine particle loss. The specimen is supported by a lower perforated plate with an opening size of 5 mm in the permeameter cell. A 5mm diameter opening is sufficient to observe the erosion of most particles within the sample, as d90 of the tested specimens is less than 5 mm, in accordance with the forthcoming display in Fig. 4.

(a)

(b)

FIGURE 2 Experimental apparatus for seepage erosion test: (a) the layout of main components of this apparatus; (b) detailed display of the rigid-wall permeameter cell

2.1.2 Soil-fluid separation testing protocol

With the assistance of the effluent collection system, the continuously collected effluent at different time intervals is stored in containers labeled with numbers after the seepage testing is completed. The effluent is a mixture of eroded silty clay particles, eroded sandy gravel particles, and seepage water. According to the seepage test by Bendahmane et al. (2008), which is conducted on clay-sand specimens, the erosion mechanism caused solely by clay particle erosion is different from the erosion mechanism where both clay and sand particles are present. Therefore, a distinction should be made between eroded silty clay particles and eroded sandy gravel particles. Moreover, the flux through the specimen should be measured to quantify the variation in hydraulic conductivity.

In order to meet the requirements mentioned above, a specific soil-liquid separation testing protocol is proposed to carry out measurements of the eroded silty clay quantity, eroded sandy gravel quantity, and seepage water volume within the effluent collected during i-th time interval. A portable light transmission meter (PLTM) (Fig. 3(a)) is used to measure the silty clay particle mass suspended in the effluent since they are too small to obtain its mass using a weighing method. This method works based on the association of the transparency of the effluent with the concentration of silty clay particles in the effluent. Thanking a previous light transmittance calibration for different silty clay concentrations (Fig. 3(b)), the PLTM can quantify the silty clay erosive concentration within the effluent. The silty clay content nci determined by the PLTM during the i-th time interval is expressed in the form

(1)

where mci is the mass of silty clay particles within the effluent obtained in the time interval i; and mwoi is the mass of the seepage water within the effluent obtained in the time interval i.

The total mass of the effluent mti obtained in the time interval i can be directly obtained by weighing and is given as

(2)

where msi denotes the erosive mass of sandy gravel particles within the effluent obtained in the time interval i.

A glass filter with a vacuum pump (Fig. 3(c)) serves to completely separate the seepage water and the eroded soil grains from the effluent, by which the mass of the seepage water mwoi and the total mass of the eroded soil particles can be measured. In this way, it is easy to obtain the eroded silty clay quantity, eroded sandy gravel quantity, and seepage water volume within the effluent obtained the i-th interval according to Eqs. (1)-(3). The experimental approach to obtaining key parameters, such as nci, mti and mwoi, will be elaborated in detail in the subsequent subsection.

The erosive mass rates per unit surface of silty clay particles, sandy gravel particles, and seepage water are respectively defined as:

(4a)

(4b)

(4c)

respectively, where s is the sample’s cross-sectional area, and ti is the duration of the interval i.

The sum of the masses of eroded soil grains measured in each time interval gives the total mass of the eroded solids during the test, that is

(5a)

(5b)

with n representing the number of time intervals divided throughout the entire experimental process, mc and ms are the cumulated eroded silty clay and sandy gravel mass, respectively.

(a)                                        (b)

(c)

FIGURE 3 Soil-fluid separation testing protocol: (a) photo of the portable light transmission meter; (b) light transmittance calibration curve for different silty clay contents; (c) photo of the glass filter with a vacuum pump

2.2 Tested material

The tested WGLS material used in this study is extracted from the Kucaoping slope deposits in Fengjie County, Chongqing, China, caused by the heavy rainfall in 2015 (Tian, 2018; Tian et al., 2020a). Due to the limitations of the size of the experimental apparatus, coarse particles larger than 10mm are removed. The wet sieving method suggested by ASTM (2018) is used to measure the grain size distribution (GSD) of the selected original soil, as shown in Fig. 4. According to the boundary diameter of 0.075 mm, the original soil is separated into pure silty clay fraction and pure sandy gravel fraction, whose GSD curves are also plotted in Fig. 4. The grain density, plasticity limit, liquidity limit, and standard optimum water content for the pure silty clay fraction are identified as 2.63 × 103 kg/m3, 25%, 57.2%, and 27.2%, respectively. The pure sandy gravel particles are classified as angular to sub-angular material. Their grain density is measured as 2.65 × 103 kg/m3. In the pure sandy gravel fraction, particles with the size of 0.075-0.25 mm are absent. The pure sandy gravel particles are classified into 5 different portions according to their particle sizes: 0.25-0.5 mm, 0.5-1.0 mm, 1-2 mm, 2-5 mm, and 5-10 mm. These pure silty clay particles and classified sandy gravel particles are used to reconstitute specimens following the GSD shown in Fig. 4.

FIGURE 4 Grain size cumulative curve of the selected original soil, pure silty clay fraction, and pure sandy gravel fraction

Empirical criteria have been proposed by researchers (US Army Corps of Engineers, 1953; Kezdi et al., 1979; Kenney & Lau, 1985; Burenkova et al., 1993) to evaluate the potential for internal instability of granular material based on the shape of the gradation curve. The results of the evaluation of the GSD studied herein are listed in Table 1. All criteria indicate that the tested soil mass is internally unstable. It should be noted that these geometric criteria are designed for cohesionless soils. The extent to which these empirical criteria for internal stability may be applied to WGLS composed of fines less than 0.075 mm is uncertain. Additionally, these methods evaluate the potential for internal instability according to a geometric constraint, namely the ability of the coarser particles to hinder the migration of fine particles. They do not provide any insight into the nature of internal erosion or the hydro-mechanical conditions triggering the onset of internal erosion. Hence, it is highly necessary to perform seepage erosion tests on the specimens to reveal the erosion behavior of WGLS.

Table 1 Assessment of the vulnerability of the WGLS to internal erosion

| Methods of evaluating the potential of for internal instability |  |  |
| --- | --- | --- |
| Method | Criterion | stability |
| US.Army | Cu<20 | U |
| Kezdi |  | U |
| Kenney&Lau | (H/F)>1(F<20%，F<30%) | U |
| Burenkova |  | U |

U denotes instability

is grain size finer than which the soil weight by percentage is 15% for coarse fraction, and  is grain size finer than which the soil weight by percentage is 85%, wherein the coarse fraction and fine fraction is obtained by splitting grain size distribution at any arbitrary grain size.

F denotes the mass fraction of grains whose diameter is smaller than a specific grain diameter D, H denotes the mass fraction of grains whose diameter is between D and 4D.

2.3 Experiment procedure

2.3.1 Specimen preparation

The specimen preparation includes two procedures: (1) material mixing and (2) compaction in layers. The repeatability of the reconstitution can be accomplished using these two procedures.

(1) The oven-dried weight of sandy gravel particles of different sizes is determined according to the GSD and desired relative density. De-aired water is added to the oven-dried sandy gravel particles and mixed sufficiently to the optimum moisture content of 5.7%. As the mixing continues, silty clay particles with an optimum moisture content of 27.2% are progressively added, and mixing is continued until visual uniformity is observed. Before compaction, the well-mixed wet test material is divided into five parts and is kept inside a zipped plastic bag for moisture equalization for 24 h.

(2) In this study, the moist tamping technique (Ladd, 1978; Forst and Park, 2003), which highlights the considerable effect of the compaction of the succeeding layers on the excessive densification of the underlying layers, is used to prevent soil segregation during compaction. The soil specimens are compacted into five layers. A non-linear average undercompaction criterion shown in Fig. 5, which has been validated by several researchers (Jiang et al., 2003; Ke and Takahashi, 2014), is used, wherein the undercompaction denotes the extent to which a layer should be less dense than the desired value. After placing the test material required for each layer into the mold, each layer is compacted manually to the height determined by the desired density and undercompaction (Fig. 5).

FIGURE 5 Average undercompaction and desired height after initial tamping of each layer

2.3.2 Internal erosion test

After installing the reconstituted specimen in the newly developed fixed-wall permeameter, the unidirectional downward seepage erosion test begins at a constant injection rate. The seepage erosion test begins with a stage of saturation. Open the peristaltic pump and inject de-aired water from the upper reservoir into the standing pipe at an extremely low infiltration rate to saturate the specimen. The purpose of adopting this low infiltration rate is to prevent the unintended migration of fine particles before the start of the erosion test. After the discharge rate stabilizes, continue the low-rate infiltration process for 2 hours to ensure the saturation of the specimen. Afterward, the inflow rate is adjusted to a predetermined value to initiate seepage erosion. During the erosion process, the weight of the upper and lower reservoirs is continuously recorded through the data collection system. Meanwhile, the designed effluent collection system is employed to precisely collect the effluent with eroded soil grains at predetermined time intervals. The entire duration of the experiment is divided into different time intervals ranging from 1 min to 5 min, with the shortest intervals of 1 min when distinct discoloration of the effluent is observed and the longest intervals of 5 min when the effluent is visually clear. The erosion tests are continued until the following criteria are satisfied: (1) the effluent is observed to be visually clear over a period of at least 10 min, and upstream hydraulic pressure remains stable; (2) the water table in the standing pipe declines drastically to zero or a minimal value; (3) the duration of test exceeded the specified time of 90 min. The average hydraulic gradient imposed on the specimen during the i-th time interval takes the following form

(6)

where mwi is the mass of the seepage water accumulated in the standing tube before time interval i;  is the standing tube’s cross-sectional area;  is the density of the seepage water;  and  is separately the change in mass of the seepage water in the upper and lower reservoir within the m-th time interval;  is the mass of seepage water exiting from the lower surface of the specimen within the m-th time interval; mwsi is the mass of the seepage water within the sample within the i-th time interval which is negligible compared to mwi.

2.3.3 Soil-fluid separation test

It is now our position to conduct the soil-fluid separation test. The separation process can be divided into three steps.

(1) These numbered containers collecting effluent at different time intervals (Fig. 6(a)) are weighted to determine the mass of the effluent.

(2) After thoroughly stirring the effluent with a glass rod, the suspension liquid is carefully dumped into a specifically designed rectangular solid box made of transparent acrylic plates to measure the concentration of silty clay particles by utilizing the PLTM, as shown in Fig. 6(b). After that, the suspension liquid is returned to the containers. It is worth emphasizing that it is necessary to add a measured quantity of de-aired water to the suspension liquid to decrease the concentration of silty clay particles when the concentration is too high to exceed the range of the PLTM. In this way, the method proposed herein can measure the concentration of effluent containing silty clay particles at any concentration, thus overcoming the limitations of the method utilized by Bendahame (2008).

(3) A glass filter is employed to separate the seepage water and eroded soil grains from effluent. After filtering, the eroded soil particles remain on the filter paper while the seepage water permeates into the conical flask. The mass of seepage water and eroded soil grains can be obtained by weighing the oven-dried filter papers (see Fig. 6(c)) and the conical flask, respectively.

FIGURE 6 Key experimental operation for soil-fluid separation: (a) the photo for numbered containers collecting effluent; (b) the photo for measuring the concentration of clay particles; (b) the photo of oven-dried filter papers used for measuring the total eroded soil mass.

2.4 Experiment scenarios

In this experiment, these tests are controlled by different injection flow rates, i.e., 25 ml/min, 39 ml/min, 56 ml/min, and 74 ml/min, and different initial porosities, that is 0.35, 0.4, 0.45, and 0.5. The details of the experimental program consisting of 7 tests are presented in Table 2. All the specimens used in these experiments are prepared with the same materials and the same specimen preparation methods. These injection flow rates are chosen from previous trial and error, at which significant erosion phenomena can be observed within 90 min. Notably, these injection flow rates used in this study are higher than the rainfall intensity observed in actual working conditions. However, compared to laboratory soil columns subjected to unidirectional seepage, the soil under field conditions is more susceptible to internal erosion. It is because more erodible particles in the soils at the field site are exposed in the exit paths of the network of interconnected pore channels due to the tortuous seepage path in various directions (Xiao & Shwiyhat, 2012). Therefore, it is reasonable to use higher infiltration rates in indoor soil column experiments to initiate erosion to some extent.

Table 2 Main characteristics of the tests

| Test code | Dry weight /g | Dry density /kg/m3 | Initial porosity | Inflow rate /ml/min | Duration (min) |
| --- | --- | --- | --- | --- | --- |
| T-0.45-25 | 159 | 1.66×103 | 0.45 | 25 | 75 |
| T-0.45-39 T-0.45-56 T-0.45-74 T-0.35-39 T-0.4-39 T-0.5-39 | 162 161.5 158 188.5 174 145 | 1.69×103 1.68×103 1.65×103 1.96×103 1.81×103 1.51×103 | 0.45 0.45 0.45 0.35 0.4 0.5 | 39 56 74 39 39 39 | 70 90 90 65 90 30 |

3 TEST RESULTS AND DISCUSSION

3.1 Temporal progression of internal erosion

The temporal progression of internal erosion in the tests is described primarily through the variations in the erosive mass rates of silty clay particles and sandy gravel particles, the transient hydraulic gradient, and the transient hydraulic conductivity with increasing test duration. According to Darcy’s law, the transient permeability coefficient can be determined from the transient hydraulic gradient and outflow rate of seepage water, that is

(7)

The erosion phenomenon observed in specimen T-0.45-39 is most prominently clear and typical among all the tests conducted. Therefore, its test results are interpreted to describe in detail the temporal evolution process of internal erosion of WGLS due to rainwater infiltration. From Table. 2, the specimen T-0.45-39 under discussion has an initial porosity of 0.45 and is subjected to an infiltration rate of 39 ml/min. Based on the test termination criteria described above, the test conducted on specimen T-0.45-39 is stopped at t = 70 min due to the observation of a sharp decrease in the hydraulic gradient at the time interval of approximately 50-60 minutes, which is followed by a visually clear stage of effluent over a period of 10 min. The variations of specimen T-0.45-39 in the erosive mass rates of silty clay particles and sandy gravel particles, the transient hydraulic gradient, and the transient hydraulic conductivity are plotted against the same time axis, as shown in Fig. 7.

FIGURE 7 Chang of silty clay particles erosion rate, sandy gravel particles erosion rate, hydraulic gradient, and hydraulic conductivity with time

3.1.1 General features of internal erosion

Internal erosion has occurred, manifested by the loss of finer particles consisting of silty clay particles and sandy gravel particles, and fluctuation in transient hydraulic gradient and transient permeability coefficient. The variation in the erosive mass rate of silty clay particles with time during the entire process directly indicates that the internal erosion is intermittent due to episodic particle migration and redeposition of finer fractions within the interstices of the matrix formed by the coarser fraction. A similar trend can be observed for the erosive mass rate of sandy gravel particles. The onset of the erosion of silty clay particles is at t ≈ 2 min, which is earlier than that of sandy gravel particles. It indicates the fact that the susceptibility of silty clay particles to internal erosion is higher than that of sandy gravel particles, which is consistent with the results by Bendahamne et al. (2008). After the initiation of erosion of the sandy gravel particles, the erosion rate of the silty clay particles changes almost synchronously with that of the sandy gravel particles. The variation in the transient hydraulic gradient with time is opposite to that of the transient hydraulic conductivity, which is theoretically determined by Equation (7). During the decline in hydraulic permeability, there is an elevation in the transient hydraulic gradient and pronounced fluctuations in the erosion rate of soil particles. This is attributed to the fact that eroded fine particles induce clogging of constrictions among the coarse particles, consequently leading to a reduction in hydraulic permeability.

3.1.2 Temporal progression of internal instability phenomena

Utilizing a combination of erosion characteristics and supplemented by the particle migration patterns illustrated in Fig. 8, a detailed description of the temporal evolution process of internal instability phenomena is provided. Four successive stages are identified throughout the entire process of seeking an equilibrium state in the inflow rate-controlled system.

(a)                                    (b)

(c)                                     (d)

(e)

FIGURE 8 Distinct particle migration patterns: (a) loose silty clay particle diffusion in the suffusion stage; (b) loose mixed particles transportation in the suffusion stage; (c) redeposition of detached particles at pore throat in the suffosion stage; (d) migration of grains detached from the pore channel wall in the piping stage; (e) no particles transportation in the stabilized stage

(1) Suffusion stage: Based on the combined analysis of the temporal variations of the erosion characteristics, the internal erosion phenomena observed from the test initiation to an elapsed time of 34 min is classified as suffusion. In this case, the hydraulic gradient progressively increases as a parabola to a nearly constant value of 1.1 m/m until an elapsed time of 11 min, followed by a tiny increase of 0.09 m/m until t= 34 min. The hydraulic conductivity is almost constant with time in this stage, with a faint decrease from 0.055 cm/s to 0.042 cm/s, which confirms a period of relative stability to an elapsed time of approximately t = 34 min. The behavior implies the onset of a slow and subtle migration of soil grains within the specimen, which is validated by the temporal development of the erosive mass rates of silty clay particles and sandy gravel particles in this stage.

The particle migration pattern shown in Fig. 8 is very useful for interpreting these test data. Upon water infiltration into the interstices of the matrix formed by the coarser fraction, the silty clay particles initially loosely deposited in the interstice foremost undergo diffusion, as shown in Fig. 8(a). As a result, the loss of silty clay particles is observed almost from the beginning. As the hydraulic gradient rises, the hydrodynamic forces exerted on the loose sandy gravel particles reach a magnitude sufficient for migration (see Fig. 8(b)). Consequently, the erosion and subsequent loss of the mixture of silty clay and sandy gravel particles are observed after the initiation of silty clay erosion. The erosion of particles initially loosely deposited in the interstice does not significantly alter the network of interconnected pore channels, thereby resulting in a relatively slow and small variation in permeability. These responses of the specimen are consistent with the phenomenon of suffusion as described by Kovacs (1981).

(2) Suffosion stage: The internal erosion phenomenon observed between 34 min and 47 min is identified as suffosion. Internal erosion by suffosion is characterized by significant changes in all of the erosion characteristics. Specifically, the transient hydraulic gradient exhibits a continuous upward trend, reaching its maximum value of 2.72 at the end of this stage. Conversely, a significant and rapid decrease in hydraulic conductivity occurs from 0.042 cm/s to the minimum value of 0.011 cm/s over the entire stage. The eroded soil grains consist of silty clay particles and sandy gravel particles. The erosive mass rates of both types of soil particles exhibit fluctuating growth. Concretely, the silty clay particles reach their maximum erosive mass rate of 1.04 × 10-3 g/(cm·s) at about 47 min, while the sandy gravel particles arrive at their maximum erosion rate of 1.36 × 10-3 g/(cm·s) approximately at 47 minutes.

The particle migration pattern in the form of redeposition of detached particles at the pore throat (Fig. 8(c)) is responsible for these pronounced variations in these erosion characteristics. Once the eroding process of loosely deposited soil particles in the pore channels is complete, the persistent hydraulic load gradually dislodges the soil particles from the soil matrix. Some of the detached soil particles are transported downstream by the water flow, while the others are entrapped at the pore throats. The washout of soil particles resulted in a dramatic increase in the erosion rate. The redeposited soil particles at the pore throats cause a reduction in the throat size, leading to a sustained decrease in the permeability coefficient. Given the condition of a constant inflow rate, the hydraulic gradient will persistently increase. It should be emphasized that particle detachment, transport, and redeposition processes occur concurrently during this stage. However, particle redeposition predominates, leading to the designation of this particle migration pattern as redeposition of detached particles at the pore throat. The phenomenon accords well with internal erosion by suffosion (Moffat et al., 2011). The suffosion results in the formation of voids and potential pathways for further erosion.

(3) Piping stage: Immediately following the suffosion stage, internal erosion takes the form of piping at 47 min< t <60 min. In this stage, a significant change also takes place in erosion characteristics, but in the opposite way to that in the suffosion stage. Specifically, the transient hydraulic gradient decreases from 2.72 to nearly 0 within approximately 13 min. A companion increase occurs in the transient hydraulic conductivity, with the permeability coefficient rising from 0.025 cm/s to 0.39 cm/s in the stage. The erosive mass rate of soil grains decreases with time during this stage, causing the effluent to become clear gradually. Sandy gravel particles and silty clay particles stop eroding at 54 min and 60 min, respectively.

Once the increased hydraulic gradient due to suffosion failure surpasses a critical threshold, the accumulated soil particles at the pore throats begin to undergo gradual erosion and are subsequently entrained by the seepage flow, resulting in a gradual increase in the size of the pore throats and the development of preferential flow paths through the eroded pore throats. Consequently, there is an onset of increased permeability, a decrease in hydraulic gradient, and a higher rate of soil particle erosion is observed during the early stage. The continued seepage flow will further dislodge soil particles from the soil matrix and expand the pore throats and channels, causing the pores to be increasingly connected to each other and forming preferential leakage channels, as shown in Fig. 8(d). As a result, the transient hydraulic gradient rapidly decreases to an extremely low value, accompanied by intermittent erosion of soil particles. These features demonstrate that piping or concentrated leakage develops within the specimen.

(4) Stabilization stage: No additional eroded soil grains are detected in the effluent over a period of 10 min after the piping stage ends. The hydraulic gradient and conductivity remain essentially constant with time in the latter stage of this phase, confirming that a state of equilibrium has been achieved. As shown in Fig. 8(e), the seepage flow within this preferential pathway formed by strong piping no longer segregates soil particles from the matrix soil. It should be noted that the rapid decrease in hydraulic conductivity and the accompanying increase in the hydraulic gradient in the early stage of this phase is attributed to refilling the preferential pathway through episodic particle rearrangement. At the end of the stabilization stage, the permeability of the specimen is approximately 0.21 cm/s, which is four times the initial permeability of 0.055 cm/s. This is because the aforementioned internal erosion behavior increases the connectivity of adjacent pores, forming expanded flow pathways within the specimen to balance the inflow rate control system.

3.1.3 Erosion evolution with respect to hydraulic gradient

Through seepage tests conducted on cohesive specimens made of sand and clay, Bendahmane et al. (2008) demonstrated the existence of a secondary critical gradient, below which only the erosion of small quantities of clay particles is observed, beyond which both clay and sand transportation is initiated. Similar findings can be found in the literature (Chang & Zhang, 2011). In their study, two critical hydraulic gradients are defined, i.e., the initiation hydraulic gradient at which the first sign of internal erosion appears and the skeleton deformation hydraulic gradient beyond which sudden increases in the erosion rate and soil permeability are observed.

Compared to previous studies, the current research allows for a more detailed delineation of the critical hydraulic gradient throughout the entire erosion process by interpreting the erosion evolution with respect to the hydraulic gradient. Specifically, six critical hydraulic gradients are identified, which correspond to the onset of different internal erosion behavior. Fig. 9 shows the evolution of the cumulative mass of the eroded silty clay particles and eroded sandy gravel particles versus the corresponding transient hydraulic gradient in the context of the entire erosion process.

FIGURE 9 Evolution of the cumulative erosive mass of silty clay particles and sandy gravel particles versus the hydraulic gradient

Before piping occurs, the cumulative erosive mass of both eroded soil grains increases with increasing hydraulic gradient. A significant increase in the cumulative erosion mass is observed even though the hydraulic gradient decreases after piping is initiated, which is consistent with the variations in the erosive mass rate of soil particles, as depicted in Fig. 7. Upon completion of the internal erosion, approximately 8 g of eroded silty clay particles and approximately 9 g of eroded sandy gravel particles are collected. The six critical hydraulic gradients are as follows:

(a) At i= 0.5, the erosion of silty clay particles is initiated in the form of suffusion, which is indicated by the onset of an increase in the cumulative erosion mass of the silty clay fraction. The hydraulic gradient of 0.51, iuc, is defined as the suffusion initiation critical hydraulic gradient of silty clay particles.

(b) At i= 1.0, the first sign of the erosion of sandy gravel particles appears in the suffusion stage. The hydraulic gradient of 1.03, ius, is referred to as the suffusion initiation critical hydraulic gradient of sandy gravel particles.

(c) At i = 1.1, a slight decrease in the hydraulic gradient occurs in the absence of soil particle erosion, which is immediately followed by similar and simultaneous sharp increases in the cumulative erosion masses of both silty clay particles and sandy gravel particles with increasing hydraulic gradient. It is indicated the start of the suffosion stage. Because of the similarity in the erosion behaviors of silty clay particles and sandy gravel particles in the suffusion stage, no distinction is made between their critical hydraulic gradients. Thus, a hydraulic gradient of 1.1 is called the suffosion critical hydraulic gradient, io.

(d) At i= 2.7, the hydraulic gradient starts to decrease while the cumulative erosion mass of both types of soil particles increases, indicating that piping commences. Again, the cumulative erosion mass curves of these two types of soil particles exhibit similar changes. Therefore, their critical hydraulic gradients are not differentiated in the piping stage. In this way, the hydraulic gradient of 2.7, ip, is called the piping initiation critical hydraulic gradient.

(e) When the hydraulic gradient falls back to 1.0, the end of the erosion of sandy gravel particles is observed for the first time in the stabilization stage. Correspondingly, the hydraulic gradient of 1.0, iss, is called the stabilization initiation critical hydraulic gradient of sandy gravel particles. Interestingly, iss is approximately equal to ius.

(f) When the hydraulic gradient declines to 0.55, the erosion of silty clay particles ends. Therefore, the hydraulic gradient of 0.55, isc, is called the stabilization initiation critical hydraulic gradient of silty clay particles, and isc and iuc are approximately equal.

It is worth emphasizing that the erosion behavior of silty clay particles exhibits similarities to that of sandy gravel particles, differing primarily in terms of the initiation time of the suffusion and stable phases. Furthermore, the cumulative erosive mass within these two phases is negligible compared with the other stages. Henceforth, they will be treated indistinguishably for the sake of descriptive convenience in the subsequent discussion.

3.2 Effect of the inflow rate on the internal erosion process

As an external driving factor for internal erosion within the current system, it is essential to study the influence of the inflow rate on the internal erosion process of soil. As shown in Table 2, seepage tests are conducted on identical specimens at inflow rates of 25 ml/min, 39 ml/min, 56 ml/min, and 74 ml/min, respectively. The seepage test on specimen T-0.45-25 is terminated at t = 75 min, while seepage tests conducted on specimens T-0.45-56 and T-0.45-79 stop at t = 90 min based on the test termination criteria described above. Fig. 10 shows the evolution of cumulative erosive mass as a function of time and hydraulic gradient for four different inflow rates.

(a)

(b)

Fig.10 Evolution of cumulative erosive mass of soil grains against (a) time and (b) hydraulic gradient for four different inflow rates

Fig. 10(a) indicates that a lower inflow rate delays the onset of particle erosion. The onset times of particle migration for the different inflow rates are 20, 18, 8, and 5 min for rates of 25, 39, 56, and 74 ml/min, respectively. It is easy to shed light on this observation. A higher inflow rate for specimens with the same permeability conductivity will result in a higher hydraulic gradient applied to the specimen at the same moment. Indeed, the hydraulic gradient is precisely the fundamental cause that triggers internal erosion.

Fig. 10(b) shows that the suffusion initiation critical hydraulic gradient iu has no relation to the inflow rate for identical specimens, with values of 0.9, 1.0, 1.1, and 1.0 m/m for rates of 25, 39, 56, and 74 ml/min, respectively. In fact, iu corresponds to the initiation of the migration of particles loosely deposited in the pore channel, as shown in Figs. 8(a) and 8(b). Theoretically, the hydraulic gradient required to initiate particle erosion should be consistent across these infiltration rates. The nearly identical iu detected in the four specimens confirms that the resistance to suffusion, an inherent characteristic of granular material, is irrespective of the inflow rate. In turn, this phenomenon confirms the effectiveness of the newly proposed experimental device and soil-fluid separation scheme and the correctness of the experimental procedure adopted in the current study.

In contrast with iu, the suffosion initiation critical hydraulic gradients io increase with the inflow rate, but the corresponding cumulative erosion mass associated with io remains nearly the same for different inflow rates. Specifically, the io and cumulative erosion mass for inflow rates of 25, 39, 56, and 74 ml/min are 1.0, 1.1, 2.0, 2.6, and 2.3, 2.5, 2.2, 2.3 g, respectively. As shown in Fig. 8(c), the io corresponds to such a critical state where loose soil particles accumulated within the pore channels are completely eroded, and dislodgement of matrix soil initiates. Therefore, it is evident that the cumulative erosion mass corresponding to io remains the same for different inflow rates.

The inflow rate significantly impacts the erosion process after the suffosion stage. During the process of seeking the equilibrium state of the infiltration rate control system, the specimen with an inflow rate of 25 ml/min only undergoes the suffosion stage without experiencing the piping stage, the specimen with an inflow rate of 39 ml/min experiences a complete coupled suffosion and piping stage (referred to as S-P stage in Fig. 10(b)), while specimens with inflow rates of 56 ml/min and 74 ml/min undergo two occurrences of the S-P stage due to continued seepage flow after suffosion. Furthermore, it can be anticipated that these two specimens require more occurrences of the S-P stage to reach the ultimate equilibrium state. Certainly, it also implies that these two specimens will suffer more severe erosion damage when they reach the final equilibrium state.

3.3 Effect of the initial porosity on the internal erosion process

The initial porosity is universally recognized to have a significant effect on the physical and mechanical characteristics of the soil; therefore, studying its effect on the internal erosion process is essential. To this end, seepage tests are performed on specimens prepared from the identical material and compacted to initial porosities of 0.35, 0.4, 0.45, and 0.5 at a 39 ml/min inflow rate, as shown in Table 2. The seepage tests conducted on specimens T-0.4-39 are stopped at t = 90 min, while the duration of tests on specimens T-0.35-39 and T-0.5-39 is separately 30 min and 65 min, based on the test termination criterion. In seepage tests of specimens T-0.35-39 and T-0.4-39, the maximum hydraulic gradient the experimental device can apply is reached. Plots of the cumulative erosive mass against hydraulic gradients for the four specimens with different initial porosity are shown in Fig. 11. The critical hydraulic gradients of the suffusion stage and suffosion stage and the cumulative weights of the eroded grains are summarized in Table 3.

FIGURE 11 Evolution of cumulative erosive mass versus hydraulic gradient for four different initial porosity

Table 3 Main erosion characteristics for four specimens with different initial porosities

| Test code | iu (m/m) | io (m/m) | Average hydraulic (m/m) | Average permeability (cm/s) | Cumulative erosive mass (g) | Mass loss rate (%) |
| --- | --- | --- | --- | --- | --- | --- |
| T-0.35-39 T-0.4-39 T-0.45-39 T-0.5-39 | 4.7 3.1 1.0 0.2 | / / 1.1 / | 5.5 5.1 1.3 0.5 | 0.0116 0.0122 0.0636 0.1227 | 0.5 2.1 17 0.45 | 0.26 1.2 10.5 0.34 |

Fig. 11 and Table 3 indicate that iu decreases as the initial porosity increases. It is because the erosion resistance of loose soil particles in pore channels is lower in samples with high initial porosity. Except for the seepage test conducted on specimen T-0.45-39, coupled suffosion-piping stage does not occur in the other tests, causing the cumulative soil particle erosion mass of sample T-0.45-39 to be significantly greater than that of the other samples. According to the mass loss rate, the potential for the internal stability of sample T-0.45-39 is lower than that of the other samples. At this point, three anomalies arise. (1) when comparing specimen T-0.45-39 with specimen T-0.5-39, the result suggests that, somewhat counter-intuitively, reducing the initial porosity may not necessarily result in higher erosion potential; (2) no correlation exists between the accumulated mass loss rate and the initial porosity; (3) more significant internal erosion is expected to take place in specimens T-0.35-39 and T-0.4-39 subjected to higher average hydraulic gradients (see Table 3) if assessed solely based on the hydraulic gradient.

Before explaining these anomalies, it should first be noted that the detachment and transportation of particles result from the hydrodynamic force imposed on the particles by interflow (Khilar 1998). The hydrodynamic force generated by the pore fluid is referred to as the hydraulic shear stress, , and is believed to be a function of the hydraulic gradient, intrinsic permeability, and porosity (Reddi et al., 2000). It takes the following form

(8)

where  is the pressure drop resulting from the seepage; is the height of the specimen;  is the average hydraulic gradient; n is the porosity; and K is the intrinsic permeability, which is determined by

(9)

where k is the Darcy coefficient of permeability;  is the dynamic viscosity; and  is the unit weight of water.

Fig. 12 shows the evolutions of the hydraulic shear stress with time for four specimens with different initial porosities, which are obtained by substituting the experimental data of the hydraulic gradient, hydraulic conductivity, and initial porosity in Eqs. (8) and (9).

FIGURE 12 Evolution of hydraulic shear stress with respect to time for four different initial porosities

The estimated hydraulic shear stress evolution can be used to shed light on these anomalies mentioned above and improve our knowledge of the fundamental characteristics responsible for internal erosion in WGLS. Specimen T-0.45-39 is subjected to the highest hydraulic shear stress during the internal erosion process. Consequently, the extent of damage induced by internal erosion is the most significant, confirmed by the largest cumulative weight of the eroded soil grains. Even though specimens T-0.35-39 and T-0.4-39 are subjected to relatively high hydraulic gradients, the relatively low hydraulic conductivities resulting from the low initial porosities (see Table 3) lead to relatively low hydraulic shear stresses and, thus relatively small amounts of damage caused by internal erosion. Specimen T-0.5-39 has the highest porosity of 0.5, thus exhibiting the highest hydraulic conductivity. Under identical infiltration rate conditions, specimen T-0.5-39 experiences the least hydraulic gradient applied to it. Therefore, its hydraulic shear stress is the lowest, responsible for the lowest cumulative weight of eroded soil grains.

The consistency between the variation in the hydraulic shear stress and that of the cumulative weight of eroded soil grains indicates a well-defined relationship between initial porosity and cumulative erosive mass is established. These results demonstrate that, in comparison to the separate utilization of hydraulic gradient and porosity for evaluating the internal stability of the soil, using hydraulic shear stress as an assessment indicator is more appropriate. This is due to the fact that internal erosion is a combined outcome of external triggering factors (hydraulic gradient) and intrinsic soil properties (permeability and porosity). Furthermore, these results also indicate that internal erosion in the soil is a highly complex process. It emphasizes that evaluating soil stability through experimental testing, rather than relying solely on empirical guidelines, is more reliable.

4 CONCLUSION

Hydrodynamically induced internal erosion in widely graded loose soils (WGLS) due to rainfall infiltration is increasingly recognized as the leading cause of geologic and geotechnical disasters in fragile mountain areas and valley terrains, such as local collapse, shallow slope failure, and debris flows. The internal erosion in WGLS is a complex process involving the separation, migration, and potential redeposition of fine particles. Therefore, it is urgent to enhance the understanding of the internal erosion process and its influencing factors to elucidate mechanisms behind internal erosion-induced geological hazards under intense rainfall conditions.

In this study, an innovative fixed-wall permeameter is designed to conduct unidirectional downward seepage tests on unconsolidated specimens at the inflow rate-controlled condition. A soil-fluid testing protocol is proposed to separate silty clay particles, sandy gravel particles, and the permeating fluid from the collected effluent. Nine soil column seepage experiments are conducted using new equipment and novel separation test methods to reveal the evolution of internal erosion and the influence of inflow rate and initial porosity of soil on the process. These conclusions are got as follows:

(1) During the entire process of seeking an equilibrium state in the inflow rate-controlled system, four successive erosion stages with different erosion mechanisms, namely, the suffusion stage, suffosion stage, piping stage, and stabilization stage, are observed based on the evolution of erosion characteristics, including the erosion mass rates of silty clay and sandy gravel particles, the hydraulic gradient, and the hydraulic conductivity.

(2) Six critical hydraulic gradients required to initiate the different erosion stages are detected during the internal erosion process by distinguishing between the stage during which only silty clay particles are eroded and the stage during which both silty clay particles and sandy gravel particles are eroded.

(3) The critical hydraulic gradient of suffusion depends on the erosion resistance of the loose soil grains within the pore channels and is, therefore, irrespective of the inflow rate. The critical hydraulic gradient of the suffosion stage increase with the increase in inflow rate. The erosion behavior during the suffosion and piping stages is significantly affected by the inflow rate.

(4) The initial porosity of the soil has an important effect on the critical hydraulic gradient of suffusion. However, specimens with high porosity do not necessarily result in severe erosion damage. It is better to use the hydraulic shear stress, which takes the initial porosity, hydraulic gradient, and hydraulic conductivity into account, to evaluate the potential extent of damage caused by internal erosion, compared to using these indicators individually.

It is worth noting that this study primarily focuses on the impact of internal erosion on the hydraulic properties of WGLS, while the investigation of its influence on the geomechanical properties of the soil is lacking. However, the latter is crucial for understanding the geological hazards caused by internal erosion and will be addressed in future research.

Acknowledgments

The work is supported by the project of science and technology research program of Chongqing Education Commission of China (No. KJQN202004306) and the Project supported by graduate research and innovation foundation of Chongqing, China ( No. CYS22050 and CYS21351).

Reference

ASTM C117-17 (2018) Standard test method for materials finer than 75-μm (no. 200) sieve in mineral aggregates by washing, Annual book of ASTM standards. ASTM International, West Conshohocken

Bendahmane, F., Marot, D., & Alexis, A. (2008). Experimental parametric study of suffusion and backward erosion. Journal of Geotechnical and Geoenvironmental Engineering, 134(1): 57-67.

Burenkova, V.V. (1993). Assessment of Suffusion in Non-cohesive and Graded Soils. Filters in Geotechnical and Hydraulic Engineering. Brauns, Heibaum & Schuler, Balkema, Rotterdam 357–360.

Chang, D.S., & Zhang, L.M. (2011). A stress-controlled erosion apparatus for studying internal erosion in soils. Geotechnical Testing Journal, 34(6), 579-589.

Chapuis, R.P., & Saucier, A. (2020). Assessing internal erosion with the modal decomposition method for grain size distribution curves. Acta Geotechnica, 15, 1595-1605.

Chehlafi, A., Kchikach, A., Derradji, A., & Mequedade, N. (2019). Highway cutting slopes with high rainfall erosion in Morocco: evaluation of soil losses and erosion control using concrete arches. Engineering Geology, 260, 105200.

Crosta, G., & Prisco, C.D. (1999). On slope instability induced by seepage erosion. Canadian Geotechnical Journal, 36, 1056-1073.

Cui, P., Guo, C.X., Zhou, J.W., Hao, M.H. & Xu, F.G. (2014). The mechanisms behind shallow failures in slopes comprised of landslide deposits. Engineering Geology, 180, 34-44.

Cui, Y.F., Jiang, Y., & Guo, C.X. (2019). Investigation of the initiation of shallow failure in widely graded loose soil slopes considering interstitial flow and surface runoff. Landslides, 16, 815-828.

Cui, Y.F., Zhou, X.J., & Guo, C.X. (2017). Experimental study on the moving characteristics of fine

grains in wide grading unconsolidated soil under heavy rainfall. Journal of Mountain Science, 14(3), 417-431.

Fannin, R.J., & Slangen, P. (2014). On the distinct phenomena of suffusion and suffusion. Geotechnique Letters, 4, 289-294.

Frost, J.D. & Park, J.Y. (2003). A critical assessment of the moist tamping technique. Geotechnical Testing Journal, 26(1), 57–69.

Gu, D.M., Huang, D., Liu, H.L., Zhang, W.G., & Gao, X.C. (2019). A DEM-based approach for modeling the evolution process of seepage-induced erosion in clayey sand. Acta Geotechnica, 14, 1629-1641.

Guo, C.X., & Cui, Y.F. (2020). Pore structure characteristics of debris flow source material in the

Wenchuan earthquake area. Engineering Geology, 267, 105499.

Guo, X.J., Li, Y., Cui, P., Zhao, W.Y., Jiang, X.Y., & Yan, Y. (2016). Discontinuous slope failures and pore-water pressure variation. Journal of Mountain Science, 13(1), 116-125.

Hu, J.B., Weng, X.L., Yang, L.X., Lei, S.M., & Niu, H.S. (2022). Centrifugal modeling test on failure characteristics of soil-rock mixture slope under rainfall. Engineering Failure Analysis, 142, 106775.

Israr, J., & Indraratna, B. (2019). Study of Critical Hydraulic Gradients for Seepage-Induced Failures in Granular Soils. Journal of Geotechnical and Geoenvironmental Engineering, 145(7), 04019025-1.

Jiang, M.J., Konrad, J.M., & Leroueil, S. (2003). An efficient technique for generating homogeneous specimens for DEM studies. Computers and geotechnics, 30(7), 579-597.

Jiang, X.G., Worman, A., Chen, X.Q., Zhu, Z.Y., Zou, Z.Y., Xiao, W.M., Li, P., Liu, G.J., & Kang, D.Y. (2023). Internal erosion of debris-flow deposits triggered by seepage. Engineering Geology, 314, 107015.

Ke, L., & Takahashi, A. (2014). Triaxial erosion test for evaluation of mechanical consequences of internal erosion. Geotechnical Testing Journal, 37(2), 347-364.

Kenney, T.C. & Lau, D. (1985). Internal stability of granular filters. Canadian Geotechnical Journal, 22, 215-225.

Kezdi, A. (1979). Soil physics. Amsterdam: Elsevier.

Khilar, K. C. & Fogler, H. S. (1998). Migrations of fines in porous media (Vol. 12). Springer Science & Business Media.

Kovacs, G. (1981). Seepage hydraulics. Elsevier, Amsterdam.

Ladd, R.S. (1978). Preparing test specimens using undercompaction. Geotechnical Testing Journal, 1(1), 16–23.

Li, J.M., Li, L., Wang, W.L., Kang, H.L., Guo, M.M., Huang, J.Q., Wang, Y.F., Lou, Y.B., Tong, X.X., & Nie, H.Y. (2023). Hydrological and erosion responses of steep spoil heaps to taproot and fibrous root grasses under simulated rainfalls. Journal of Hydrology, 618, 129169.

Li, M. & Fannin, R.J. (2012). A theoretical envelope for internal instability of cohesionless soil. Géotechnique, 62(1), 77–80.

Li, W.C., Deng, G., Liang, X.Q., Sun, X.X., Wang, S.W., & Lee, M.L. (2020). Effects of stress state and fine fraction on stress transmission in internally unstable granular mixtures investigated via discrete element method. Powder Technology, 367, 659-670.

Liang, L., Tian, D.L., Ning, Y., & Wang, X. (2020a). Experimental Investigation of Internal Stability of Widely Graded Coarse Granular Soil and Criteria of Internal Stability. Chinese Journal of Underground Space and Engineering, 16(3), 835-843. (In Chinese)

Liang, Y., Yeh, T.C.J., Ma, C., Zhang, Q., Yang, D.H., & Hao, Y.H. (2020b). Experimental investigation of internal erosion behaviours in inclined seepage flow. Hydrological Processes, 34(26), 5315-5326.

Liang, Y., Zhang, B., Yang, Y.M., Zhang, H.J., & Dai, L. (2023). Experimental investigation on erosion progression and strength reduction of gap‑graded cohesionless soil subjected to suffusion. Environmental Earth Sciences, 82, 173.

Lindow, N., Fox, G.A., & Evans, R.O. (2009). Seepage erosion in layered stream bank material. Earth Surface Process and Landforms, 34, 1693-1701.

Ma, Q.R., Wautier, A., & Zhou, W. (2021). Microscopic mechanism of particle detachment in granular materials subjected to suffusion in anisotropic stress states. Acta Geotechnica, 16, 2575-2591.

Mao, H.T., Zhang, C., He, T., & Yi, G. (2022). Influences of seepage of muddy water on the permeability of coarse-grained soil. Transactions of the Chinese Society of Agricultural Engineering, 38(9), 140-150.

Maroof, M.A., Mahboubi, A., & Noorzad, A. (2021). Effects of grain morphology on suffusion susceptibility of cohesionless soils. Granular Matter, 23, 8.

Marot, D., Regazzoni, P.L., & Wahl, T. (2011). Energy-Based Method for Providing Soil Surface Erodibility Rankings. Journal of Geotechnical and Geoenvironmental Engineering, 137(12), 1290-1293.

Moffat, R.A., Fannin, R.J., & Garner, S.J. (2011). Spatial and temporal progression of internal erosion in cohesionless soil. Canadian Geotechnical Journal, 48(3), 399-412.

Ni, H.Y., Zheng,W.M., Tie, Y.B., Su, P.C., Tang, Y.Q., Xu, R.G., Wang, D.W., & Chen, X.Y. (2012).

Formation and characteristics of post-earthquake debris flow: a case study from Wenjia Gully in Mianzhu, Sichuan, SW China. Natural Hazards 61, 317–335.

Reddi, L.N., Lee, I.M., & Bonala, M.V. (2000). Comparison of internal and surface erosion using flow pump tests on a sand-kaolinite mixture. Geotechnical Testing Journal, 23(1), 116-122.

Richards, K.S., & Reddy, K.R. (2007). Critical appraisal of piping phenomena in earth dams. Bulletin of Engineering Geology and the Environment, 66(4), 381-402.

Rochim, A., Marot, D., Sibille, L., & Le, V.T. (2017). Effects of Hydraulic Loading History on Suffusion Susceptibility of Cohesionless Soils. Journal of Geotechnical and Geoenvironmental Engineering, 143(7), 04017025.

Shire, T., O’Sullivan, C., Hanley, K.J., & Fannin, R.J. (2014). Fabric and Effective Stress Distribution in Internally Unstable Soils. Journal of Geotechnical and Geoenvironmental Engineering, 140(12), 04014072-1.

Skempton, A.W., & Brogan, J.M. (1994). Experiments on piping in sandy gravels. Geotechnique, 44 (3), 449–460.

Taha, H., Nguyen, N.S., Marot, D., Hijazi, A., & Saleh, K.A. (2022). A DEM study of the effect of the loss of fine particles on the mechanical behavior of gap-graded soils. Geomechanics for Energy and the Environment, 31, 100305.

Tian, D.L. (2018) Influence factor study of internal stability of silty clay containing rock fragments under Rainfall Infiltration, MPhil. thesis, Chongqing University, Chongqing, China. (In Chinese)

Tian, D.L., Xie, Q., Fu, X., & Zhang, J.H. (2020a). Experimental study on the effect of fine contents on internal erosion in natural soil deposits. Bulletin of Engineering Geology and the Environment, 79, 4135-4150.

Tian, D.L., Xie, Q., Ning, Y., Fu, X., & Zhang, J.H. (2020b). Experimental investigation on seepage deformation of gap-graded sand-gravel soils. Rock and Soil Mechanics, 41(11), 3663-3670. (In Chinese)

To, P., Agius, D., & Cussen, L. (2020). Influence of relative density of the granular base soil on filter

Performance. Acta Geotechnica, 15, 3621-3627.

To, P., Scheuermann, A., & Williams, D.J. (2018). Quick assessment on susceptibility to suffusion of continuously graded soils by curvature of particle size distribution. Acta Geotechnica, 13, 1241-1248.

U.S. Army Corps of Engineers. (1953). Filter Experiments and Design Criteria. Technical Memorandum. Waterways Experiment Station, Vicksburg.

Wan, C.F., Fell, R. (2008). Assessing the potential of internal instability and suffusion in embankment dams and their foundations. Journal of Geotechnical and Geoenvironmental Engineering, 134(3), 401-407.

Wang, Z.B., Wang, R., Hu, M.J., Chen, N.Y., & LÜ, S.Z. (2011). Effects of particle transport characteristics on permeability of soils from Jiangjiagou ravine. Rock and Soil Mechanics, 32(7), 2017-2024. (In Chinese)

Wang, Z.B., Li, K., Wang, R., & Hu, M.J. (2016) Impact of fine particle content on mode and scale of slope instability of debris flow. Advances in Science and Technology of Water Resources, 36(2), 35-41. (In Chinese)

Xiao, M., & Shwiyhat, N. (2012) Experimental investigation of the effects of suffusion on physical and geomechanic characteristics of sandy soils. Geotechnical Testing Journal, 35(6), 890-900.

Xiao, Y., Ma, G.L., Wu, H.R., Lu, H.M., & Zaman, M. (2022). Rainfall-Induced Erosion of Biocemented Graded Slopes. International Journal of Geomechanics, 22(1), 04021256.

Yin, Y.Z., Cui, Y.F., Liu, D.Z., & Lei, M.Y. (2019). Study on Microscopic Process of Fine Particle Migration in Loose Soil. Advanced Engineering Sciences, 51(4), 21-29. (In Chinese)

Yuan, G.L., & Che, A.L. (2022). Evolution and spatio‑temporal characteristics of slope erosion due

to rainfall in Southwest China. Bulletin of Engineering Geology and the Environment, 81, 270.

Zhang, Z.P., Fu, X.D., Sheng, Q., Du, Y.X., Zhou, Y.Q. & Huang, J.H. (2021). Stability of Cracking Deposit Slope Considering Parameter Deterioration Subjected to Rainfall. International Journal of Geomechanics, 05021001-1.

Zhu, Q., Su, L.J., Liu, Z.Y., Yang, S.H. (2021). Study of seepage in wide-grading soils with particles migration. Rock and Soil Mechanics, 42(1), 125-134. (In Chinese)

Corresponding author: D.L. Tian at School of Civil Engineering, Chongqing University, Chongqing, PR China. Email: tiandalang135@163.com