HTGB and HCI stress induced variability in the nanowire Si MOSFETs

Abderrezak BEKADDOUR and Gérard GHIBAUDO

This paper presents the room temperature performance of Si MOSFET nanowires subjected to NBTI (Negative Bias temperature Instability) and HCI (Hot Carrier Injection) stress. The static and dynamic characterizations were carried out with an enormous amount of stress adequate for a trapping / detrapping corresponding to NBTI and HCI. A simulated aging test bench has been designed to evaluate the lifetime of trapping / detrapping loads under resistive stress with an ambient temperature of 300K.

1-INTRODUCTION:

The development of a new range of consumer applications for the data storage has led to the appearance of new challenges in the already very competitiveness of memories, from “mass” memories (Flash, hard disk) to memories embedded in new electronic circuits. And the 'classic' memories now have to deal with increasingly critical technological problems due to downscaling  constraints [1][2].

In order to continue improving the performance of flash memories while reducing production costs, it is necessary to continue their miniaturization. With the reduction in the size of memory cells, new specific issues appear, in addition to the inherent limitations of the MOS transistor. They concern mainly the thickness of the dielectrics, and in particular that of the tunnel oxide which, when it is too thin (<8nm), is no longer sufficiently insulating, which leads to discharge premature cell and therefore poor retention. In order to overcome this difficulty, one solution consists in replacing the continuous floating gate with a discrete floating gate, thus limiting unloading to the trapped charges located opposite the defect in the oxide[3].

This discretization can be achieved by using a network of nanocrystals. Of much research has been conducted on the fabrication and integration of nanocrystals in silicon (SI), from which resulted several demonstrators of memory matrices and even commercial products using this technology (Freescale). However, the weak point of silicon nanocrystal memories is their small programming window [16].

On the other hand, for half a century, electronics have used silicon components. Although improvements continue to be made, silicon technology is now reaching asymptote limit, especially with regard to trapping performance [2][1]. This is why researchers have turned to a new simulator such as quantum transport, which pushes the limits of trapping in three directions i.e. transport, device width and depth directions [2]. Thanks to its simplicity to optimize and the advantage of being normally controlled,nanowire MOSFET in silicon has become one of the most serious candidates to substitute conventional MOSFETs or IGBTs in silicon [4][3]. In addition, recentstudies have shown that gate oxide is reliable up to 500K but oxide trapping is still a major issue in MOSFETs compared to JFET and BJT structures[5].

Various electronics applications are susceptible to reliability issues due to trapping / detrapping phenomena [2]. For all these applications, researchers are turning to quantum transport simulators which must ensure smooth running and sufficient reliability for the device operation[7][6].

.

The objective of this article is to present the performance of Si nanowire MOSFETs in the presence of NBTI and HCI inducedtrapping for industrial application[8]. For this, the static and dynamic characterizations were carried out at room temperature (300K) as well as an aging test under aeronautical conditions and also in nuclear reactor control rooms [9]. This makes it possible to estimate the performance (lifetime yield) that can be achieved at the level of the inverter.

2-THE ADVANTAGE OF THE FOURIER TRANSFORM:The switching characterizations of the nanowire MOSFET in silicon were simulated at 300K. In our study, the switching simulation was carried out under the same conditions for the ambient temperature in order to observe an evolution of the trapping charges and also under the effect of the drain voltage variation atrelatively high value, approximately 0.15 V for the nanowire Silicon MOSFET.

On the other hand, we have modeled the quantum transport phenomenon after solving the Schrödinger and the Poisson equations. The Fourier transform technique was applied on the Schrödinger equation to analyze the trapping phenomena as a function oftime. Only this technique was keen to handle statistical study of the final trapping effect.Using the theorems of statistical physics allowed us to give a final description of the trap phenomenon coming from the NBTI and HCI stress and also always under the effect of high value of polarization of the drain-source.

Currently, researchers are trying to improve the simulation procedure for the nanowire MOSFET in order to increase the reliability of the component, particularly with regard to the gate oxide. It is possible to find studies with conflicting opinions on the reliability of Si nanowire MOSFETs. In [10] and [11] the authors show a degradation of the threshold voltage whereas more recently [12] and [13] the authors demonstrate a good lifespan with a stable characteristics. Here we will focus our study on the evolution of the electrical parameters intrinsic to the silicon nanowireMOSFET [19][20]. Note that the reliability of the SiO2-Si oxide interface is the limiting point of the MOSFET.

Our aging study is divided into three parts: i) first an accelerated aging with fixed gate voltage and High temperature Gate Bias (HTGB), ii) then a switched gate voltage Bias Instability and iii) to finish with a Time-To-Failure for an application providing the lifetime of the nanowireMOSFET.

3-ANALYSIS OF THE ROBUSTNESS OF NANOWIRE MOSFET.

The instability of the threshold voltage is linked to the additional activation of traps, «near-interfacial oxide traps», or even the creation of additional interface charges that modify the threshold voltage. This instability was observed independently of the temperature. So we can link this problem to the injection of carriers.

Several phenomena can explain the injection of carriers. The main phenomenal are: the tunnel effect, the Fowler-Northeim injection and the injection of hot carriers.

In particular, the “High Temperature Gate Bias (HTGB)” is used to assess the reliability of the nanowireMOSFET. On the other hand, for HTGB, the threshold voltage of the nanowire MOSFETcan be more stable. We will show that in the case of a pulsed biasexcitation, the derivative of the threshold voltage VTH can be lower and is not as high as in HTGB DC standard.

Therefore, the HTGB DC standard is unlikely to be representative of actual operation. We propose here to study the aging of the component subjected to realistic stress.

In a second step, in order to treat the stability of the threshold voltage indifferent operating modes, we will load the duty cycle of the nanowire MOSFETsand also applying a very high drain voltage.Moreover, the nanowire MOSFET is characterized before starting aging.

Fig.1Schematicview of the GAA Si-NW FET consisting of a 20nm undoped channel and 10nm SD regions nominally doped at 1020cm-3. The cross section of the devices is 5x5 nm2, and the SiO2oxide and High-κ thickness are 0.2nm, 0.8nm respectively

Fig. 2(Solid blue lines)AtMi= (xi,yi,zi) single charge  trapping ;  ID-VDS characteristics of the GAA nanowire Si-MOSFET. (Dashed magenta, red and green  lines) The smooth device is also shown for comparison at gate voltage 0.4 V, 0.45V and 0.5V respectively.

# 4-PHYSICAL MODELS:

# Numerical simulations were performed by self-consistently solving the 3-D Schrodinger and Poisson equations in the coherent transport regime in the presence of fixed charge centers trapped at the SiO2/high-κdielectric interface.

In order to reduce the numerical burden the coupled mode space (CMS) approach is used within the NEGF formalism [12][17][18]. According to the CMS approach the discrete electron correlation function reads:

G<i1,i2,j1,j2,k1,k2,E=n,mGms<i1,i2,n,m,EФi1nj1,k1Фi2m*j2,k2           (1)

whereФinn=1,2,…,NyNz is the orthonormal set of eigen-functions solution of the 2-D Schrodinger problem for the ith slice of thedevice, Gms< is the mode-space counter part of the real-space Green’s function and Ny(Nz) indicates the number of discretization nodes along the y(z) confinement direction. The solution in the transverse plane is obtained assuming close boundary conditions with vanishing wave functions at the gateoxide interface. The Green’s functions in the mode space are obtained as solution of the two kinetic equations

E-Hms-∑msGms=I                                           (2)

Gms<=Gms∑ms<Gms†

where∑ms< and  ∑ms are the lesser-than and retarded self-energies describing the ideal infinite equipotential contacts, Hms is the mode-space Hamiltonian and I is the identity matrix, for every energy E. Then the real space electron density is evaluated through the integral:

ni,j,k=-igvgsΔxdE2πG<i,i,j,j,k,k,E(3)

wheregvs are the valley and spin degeneracy coefficients, respectively.

The Poisson equation,

∇εr∇ϕr=ρr(4)

is solved in the 3-D domain using the box-integration method,whereεr is the position dependent dielectric constant,ρris total charge density accounting for both electrons and fixedcharges, and ϕr is the self-consistent electrostatic potential.

The electrical tunnel junction is an gate all around(GAA) whose value is controlled by the relative juxtaposition of the semiconductor-insulator of two electrical layers.We will focus in this paragraph on the origin of this variation and, more specifically, on electrical transport through the tunnel barrier.

The GAA Si-NW FET consistsof a 20nm undoped channel and 10nm Source-Drain regions nominally doped at 1020cm-3. The cross section of the devices is (5x5) nm2, and the SiO2oxide and High-κ thickness are 0.2nm, 0.8nm, respectively

We notice a systematic positive threshold voltage shiftdue to the additional barrier on the device subbands induced by the negatively charged defect. The current amplitude variation ΔId = Id − Idball  induced by this additional barrier can be associated to the HTGB and HCI stress for VG= 0.5V, VG=0.45V and VG=0.4V, respectively . Such that the transfer characteristics of such devices in the presence of a single trap charge located at the Si/SiO2 interface and at different positions along thex-y-z volume (seeFig. 1) are shown in Fig. 2, where the turn-on curve of a clean device is plotted as the reference.

5-ANALYSIS AND RESULTS:

The distribution of the Idball (dashed line) current is shown in Fig 2. In parallel as we discussed in [2], Id values are normally distributed and the current distribution broadens during HTGB and HCI stress. Such a trend can be seen in Fig 3, which shows that the PDF and CDF of the linear drain current increases with stress time and this behavior is typical for all stress conditions.In the simulation of Fig. 3,we applied source drain voltage VDS=10mV and various gate voltages VGS and the temperature is T=300K. The ID(VDS)outputcharacteristics of such devices in the presence of a single trap charge located at the Si/SiO2/high-κ interfaces and at different positions along the x-y-z volume are shown in Fig. 4, where the on- turn curve of a clean device is plotted as the reference.

Fig. 3At VG=0.4V, 0.45V, 0.5V PDF and the corresponding  CDF (square line points), (circle line points) and (diamond line points) respectively  with VDS =10mV versus ΔVT.

The aging test was carried out for several phenomena in order to achieve an aging law. The effect obtained for a one-time trapping phenomenon and for a temperature of 300K is about 250 hours. The obtained continuous Nt densities were also a subject for discretization / randomization [2,16]. In a similar manner as in the case of randomization discretes, we multiplied the local Nt value by the cell volume at the interface is three-dimensional though, thereby obtaining the mean number of traps which was then used in a Poisson randomizer to obtain the fluctuating number of interface traps in the cell.

To summarize, for each combination of stress voltages Vds , Vgs;  we generated 201 different configurations of  randomization discretes and then each of them, in turn, has 201 different realizations of HTGB and HCI. Therefore our ensemble contained 40401 different structures.

Based on the initial 201 instantiations with  randomizationdiscretes, we calculated ensembles of skewness and kurtosis traces and extracted corresponding device lifetimes. In Fig. 5 and Fig.6, we can clearly see that the trapping phenomenon is an accelerating factor over the service life.

The gradual doping of the channel was introduced in order to reduce the bipolar parasitic effects present in the SOIs and which cause hysteresis, instability during operation in dynamic regime, an anomaly of the slope below the threshold and degradation of the voltage of breakdown.

However, gradual doping has shown other interesting advantages, in particular on Gate all around GAA architectures such as the increase in the saturation current, the early voltage and the transductance due to the reduction in the influence of the drain on the channel and its low impact on channel saturation.

From Fig.7, there are a few materials that can provide a practical solution to leakage currents through the dielectric such as High-K characterized by better immunity to degradation from hot electrons and tolerance of stronger electric fields.

However, the Hight-K and the oxides represent a medium-term solution. Indeed, we observe an increase in the density of interface state due to the presence of oxygen or hydrogen atoms resulting from HfO2 At this level, new manufacturing processes have been developed to push the limits of these materials.

Another simpler solution is to substitute silicon oxide with a high permittivity (high-К) insulator. The large value of the dielectric constant makes it possible to decrease the equivalent oxide thickness and to increase the physical thickness of the dielectric beyond the injection length of the charge carriers by tunneling.

In addition to the permittivity, the properties included are: height of the barrier and alignment of the bands with respect to silicon, thermodynamic stability, and morphology of the film, interface quality and defect in the volume and finally compatibility of the process (material of the grid, deposition technique).

This list of criteria restricts the number of materials likely to succeed in CMOS integration, we retain HfO2, whose permittivity is close to 20 (Fig8).The mean of threshold voltage ΔVT is plotted versus Drain voltage VD in Fig.8 for different values of Nt densities and for different value of VG.

During the deposition of the dielectric, it is possible that an interface layer (SiOx) forms. This layer of unknown thickness is likely to greatly degrade the quality of the oxide interface. It is therefore more advisable to deposit a thin layer of SiO2 of known thickness and qualities, which forms an oxide stack with a lower dielectric constant and a greater barrier height.

Fig.4At VG=0.4V, 0.45V, 0.5V PDF and the corresponding  CDF (square line points), (circle line points) and (diamond line points) respectively on 120mV VDS polarization

The introduction of high permittivity insulation requires the use of a metal grid instead of polysilicon whose reactivity with certain high-К materials can cause degradation of the characteristics of the component.

The metal gate also makes it possible to avoid an additional capacity created by the phenomenon of depletion present in the polysilicon grids. Optionally, increasing the doping of the gate at the interface to mitigate the depletion can cause penetration of the dopant into the oxide (Fig.9)

Fig. 5The kurtosis and the skewness of the threshold voltage shift probability due the HTGB and HCI degradation density Nt

Fig. 6At VG=0.4V, 0.45V, 0.5V The mean and standard deviation of threshold voltage ΔVT’versus Drain voltage VDS

Fig. 7At VG=0.4V, 0.45V, 0.5V  the   kurtosis and the skewness of threshold voltage ΔVT’versus Drain voltage VD

6-CONCLUSION  If Si nanowire MOSFETs are today quite robust with a lifespan of more than several thousand hours, our simulations and the literature show that the drain current in Si nanowire MOSFETs continue to present reliability problems linked to the gate oxide.

However, the various studies lead to variable results, in particular depending on the test conditions. The degradation in charge trapping / detrapping mode is more severe than in static test (negative HTGB) which is curious and suggests that the phenomena of carrier injections exist during the switching phases induced on the trapping of charges. It is therefore necessary to continue these robustness studies to define suitable tests as well. These different analyses are dealt with in this paper.

Fig. 8At VG=0.4V, 0.45V, 0.5V the mean of threshold voltage ΔVT’versus Drain voltage VDof having a determined value of due to a given HTGB and HCI degradation density Nt

Fig. 9At low drain voltage, the mean of threshold voltage ΔVT’versusNINVof having a determined value of due to a given HTGB and HCI degradation density Nt

On the other hand, in this paper, several reliability and aging tests were carried out in order to know the lifetime of MOSFET nanowires in high temperature applications. The gate voltage levels, time and temperature are factors that will deteriorate the quality of the SiO2 –Si interface. Reliability is given to us by the instability test.

A. BEKADDOUR

abderrezak.bekaddour@univ-tlemcen.dz–

URMER Department of Physics University of Tlemcen BP 119 Fg Pasteur 13000 Tlemcen Algeria

G. GHIBAUDO

Institut de Microélectronique, Electromagnétisme et Photonique

Laboratoire d’Hyperfréquences et Caractérisation

Grenoble INP-Minatec, 3 parvis Louis Néel, BP 257.38016 GRENOBLE CEDEX 1. France

Tel +33 (0)4 56 52 95 00 ; Fax +33(0)4 56 52 95 01

References

1.  ITRS Roadmap 2009, available at www.itrs.net/Links/2009ITRS.

2. A.BEKADDOUR, M.Pala N.E Chabansarie, G.Ghibaudo, “Deterministic method to evaluate the threshold voltage variability induced by discrete trap charges in Si-Nanowire FETs” IEEE trans. Electron Devices, 59, no.5, p 1462-1467, (2012)

3. K.Matocha, G.DunneS.Soloviev and R. Beaupre, “Time-dependent ndielctric breakdown of 4H-SiC MOS capacitors and DMOSFETs” IEEE trans. Electron Devices, 55, no.8, p 1830-1834, (2008)

4L.Yang et A. Castellazzi “High temperature gate-bias and reverse-bias tests on SiC MOSFET” Microelectronics Reliability , vol. 53 pp. 1771-1773, (2013)

5. S.Poli, M.G Pala and T. Poiroux, “Full Quantum Treatment of Remote Coulomb Scattering in Silicon Nanowire FETs” IEEE trans. Electron Devices, 56, p 1191-1198, (Jun 2009)

6.  clock recovery architecture and monolithic implementation’ in Razavi, B. (Ed.): ‘Monolithic phase-locked loops clock recovery circuits’ - Wiley-IEEE Press, New York, (1996)

7.  Neha Gupta, Ajay Kumar & RishuChaujar “Impact of device parameter variation on RF performance of gate electrode workfunction engineered (GEWE)-silicon nanowire (SiNW) MOSFET” Journal of Computational Electronics volume 14, pages798–810, (2015)

8. Neha Gupta, Ajay Kumar & RishuChaujar“Oxide bound impact on hot-carrier degradation for gate electrode workfunction engineered (GEWE) silicon nanowire MOSFET” Microsystem Technologies volume 22, pages2655–2664 (2016)

## 9. Neha Gupta,  RishuChaujar “Optimization of high-k and gate metal workfunction for improved analog and intermodulation performance of Gate Stack (GS)-GEWE-SiNW MOSFET” Superlattices and MicrostructuresVolume 97, Pages 630-641, (September 2016)

## 10.Jin-Woo Han, Dong-Il Moon, Jae Sub Oh, Yang-Kyu Choi, and M. Meyyappan“Vacuum gate dielectric gate-all-around nanowire for hot carrier injection and bias temperature instability free transistor” Appl. Phys. Lett. Vol 104, Issue 25, pp 3506 (2014)

11. Pu, Xiaojuan; Wei, Ying; Li, Xiaolong; Feng, Haonan; Liang, Xiaowen; Feng, Jie; Sun, Jing; Yu, Xuefeng; Guo, Qi“Study on Total Ionizing Dose Effect of Silicon Carbide Metal Oxide Semiconductor Field-Effect Transistors at High and Low Dose Rates”   Journal of Nanoelectronics and Optoelectronics, Volume 17, Number 5, pp. 809-813(May 2022)

12. Benfdila, A.; Lakhlef, A. “Graphene Material and Perspectives for Nanoelectronics.”  Journal of Nanoelectronics and Optoelectronics, Volume 13, Number 10, pp. 1437-1443, (October 2018)

## 13. L. Yang, A. Castellazzi “High temperature gate-bias and reverse-bias tests on SiC MOSFETs” Microelectronics Reliability, Volume 53, Issues 9–11, Pages 1771-1773, (2013)

## 14.Shin-Ichiro Hayashi, Keiji Wada“Accelerated aging test for gate-oxide degradation in SiC MOSFETs for condition monitoring” Microelectronics Reliability, Volume 114, Issues 11–3, Page777, (2020)

# 15. Jimmy Franchi, Martin Domeij, Kwangwon Lee “1200 V SiC MOSFETs with Stable VTH under High Temperature Gate Bias Stress” Materials Science Forum, Vol 963,Pages: 753-756, (July 2019).

# 16.Neha Gupta, Ajay Kumar & RishuChaujar“Design Considerations and Capacitance Dependent Parametric Assessment of Gate Metal Engineered SiNW MOSFET for ULSI Switching Applications”Silicon volume 12, pages1501–1510 (2020).

# 17.Zhuoqing Yu; Zixuan Sun; Runsheng Wang; Jiayang Zhang; Ru Huang“Hot Carrier Degradation-Induced Dynamic Variability in FinFETs: Experiments and Modeling” IEEE TED Vol: 67, Issue: 4,Page(s): 1517 - 1522 (April 2020)

# 18.C. Liu, K. Taek Lee, S. Pae and J. Park, “New observations on hot carrier induced dynamic variation in nano-scaled SiON/poly HK/MG and FinFET devices based on on-the-fly HCI technique: The role of single trap induced degradation”, IEDM Tech. Dig., pp. 34.6.1-34.6.4, .(Dec. 2014).

19.  Z. Yu, J. Zhang, R. Wang, S. Guo, C. Liu and R. Huang, “New insights into the hot carrier degradation (HCD) in FinFET: New observations unified compact model and impacts on circuit reliability”, IEDM Tech. Dig., pp. 7.2.1-7.2.4, (Dec. 2017).

20. E. Seevinck, F. J. List and J. Lohstroh, “Static-noise margin analysis of MOS SRAM cells”, IEEE J. Solid-State Circuits, vol. JSSC-22, no. 5, pp. 748-754, (Oct. 1987).