Evolutionary Mechanism and Damage Characteristics of “Gel-solid” Creeping Discharge of Power Device Package Insulation Under Coupled Temperature-Frequency Effects

Jian Wang *, Haosheng Yan, Chen Chen, Wei Wang, Wei Wu, Jiajun Ye and Qingmin Li

State Key Lab of Alternate Electrical Power System with Renewable Energy Sources, North China Electric Power University, Changping District, Beijing, China

corresponding author: Jian Wang, North China Electric Power University, Beijing, 102206, China.

Email: wangjian31791@ncepu.edu.cn

Funding information: National Key R&D Program of China (2021YFB2601404)

Abstract: The multi-energy conversion equipment power devices are prone to form creeping discharges at the interface of silicone gel and ceramic substrate. In this paper, the influence mechanism of coupled temperature-frequency effects on the creeping discharge of “gel-solid” insulation and the surface damage characteristics of ceramic substrate under high-frequency electrical stress were investigated; and the influence mechanism of specimen properties on the discharge was studied based on different degassing methods. The research results showed that the partial discharge initial voltage was independent of the change in frequency, but decreased with increasing temperature. The maximum discharge amplitude and the pulse recurrence frequency increase first and then decrease with the increase of frequency, and there is the phenomenon of “frequency-induced inflection point”; the trend increases with the increase of temperature, and the increase of temperature has a certain weakening effect on the phenomenon of “frequency-induced inflection point”. Due to the nature of the material, the discharge activity of the vacuum-treated sample is slightly lower than that of the non-degassed sample. With the aggravation of surface damage and the generation of products in different discharge stages, the surface conductivity showed a gradual upward trend. The analysis concluded that the coupled temperature-frequency effects had a significant effect on the development of creeping discharge; the bubbles in the colloid and the air gap in the substrate were important factors affecting the discharge; and the creeping discharge pattern was mainly determined by the damage characteristics of the substrate.

- Introduction

IGBT (Insulated Gate Bipolar Translator), as a new type of power semiconductor device, combines the advantages of BJT (Bipolar Junction Transistor) and MOSFET (Metal-Oxide-Semiconductor Field Effect Transistor) in one, it is the core device for energy conversion and transmission of multi-energy conversion equipment, and is called the “CPU” of power electronics devices. With the advantages of high voltage, high current, high input impedance, low driving power and fast on/off speed, IGBT was widely used in rail transportation, smart grid, electric vehicles and new energy generation [1]. However, as the operating voltage and current of IGBT increases and the chip size keeps decreasing, the chip power density increases dramatically, which directly leads to greater electrical and thermal stresses on the package insulation materials, so the reliability of IGBT is a key problem that must be solved.

The main packaging insulation materials of high voltage power modules include potting insulation and substrate insulation. The potting insulation material wraps both the metal electrode and the ceramic substrate, so the metal electrode, the ceramic substrate and the potting insulation form a “triple solid” insulation structure under an inhomogeneous electric field. The metal electrodes, ceramic substrates and potting insulation “triple junction” where the electric field distortion is most serious due to the geometric structure, and partial discharge and aging phenomena tend to occur in this area and develop along the potting insulation-ceramic substrate interface (Fig. 1), eventually causing degradation of the IGBT power module insulation material [2]. Therefore, an in-depth study of the relationship between the creeping discharge and the surface damage of the insulation material provides theoretical support to further improve the reliability and accuracy of power module fault state monitoring.

FIGURE. 1.  Cross section of insulated gate bipolar transistor (IGBT) module

The degradation of insulating materials under the action of creeping discharge has been studied by a large number of domestic and foreign scholars, and some results have been achieved. Jin Wang's team at Ohio State University analyzed the effect law of rise time and repetition frequency on the onset voltage of creeping discharge of silicone gel and DBC [3]. Th. Lebey investigated the corresponding discharge types by comparing the normalized detection and the newly proposed detection results for different defect modes of IGBT, and he concluded that the basic defect mode was the main reason for distinguishing the types of partial discharges in IGBT modules [4]. Akiko Kumada's team at the University of Tokyo explored the dynamic potential on the hole surface with the help of Pockels effect to reveal the discharge mechanism of welded IGBT and investigated the relationship between the hole diameter at the end of the electric tree and the discharge pulse during the discharge process [5-7]; J.-L. Auge et al. studied partial discharges in metallized substrates embedded in silicone gels and various liquids and found that changing the substrate properties had a significant effect on PD behavior, while modification of the encapsulation material had little effect, and he concluded that partial discharges occurred within the pores present in the sintered ceramic material, rather than in the encapsulation material as was commonly believed [8-9]; Cui Xiang's team at North China Electric Power University investigated the creeping discharge characteristics of nitrogen and polyether ether ketone interfaces in rigid crimped IGBT device packages under positive repetitive square waves and found that the creeping discharge phenomenon and discharge mechanism of the package material under the action of positive square waves were significantly different from those under industrial frequency and direct voltages, forward and reverse discharge occurred in the rising edge of square wave and the high level area and the descending edge of square wave and low level area respectively [10-13]. So far, in the study of internal discharge of IGBT devices, there was no unified conclusion on the discharge evolution mechanism. The reason was that the process of “gel-solid” creeping discharge was complex, and it involved various influences such as material phase change and streamer theory, which was difficult to study. In addition, we have not seen any research on the evolution mechanism of creeping discharge of silicone gel-ceramic substrate interface and the degradation mechanism of insulating materials, and there was a lack of relevant theoretical basis and analysis.

In this paper, a column-plate electrode model with aluminum nitride as ceramic substrate in silicone gel package was designed. The creeping discharge test was carried out under frequency-dependent electric stress, and the different discharge stages were classified according to the insulation life, and the discharge parameters of different stages were counted at each frequency, and the effect of coupled temperature-frequency effects on the creeping discharge was considered. The surface morphology, surface generation and surface conductivity of different damage stages were examined using scanning electron microscopy, infrared spectroscopy, X-ray energy spectrometer and three-electrode system. The correlation between the temperature-frequency synergy effect, surface damage of insulating materials and creeping discharge was discussed.

- Test methods and measurements

- 2.1 Discharge test platform and test process

The test platform used in this paper is shown in Fig. 2, which mainly consisted of high-frequency and high-voltage source, column-plate electrode model, high-voltage probe, high-speed digital oscilloscope and UHF sensor. The high-frequency and high-voltage source could output a continuously adjustable voltage output of 0-50 kV and sinusoidal voltage with frequency range of 0-50 kHz; the UHF sensor (TWUHF-G04) had a frequency band of 200 MHz-2 GHz, a sensitivity of 1 pC and an effective height of more than 12 mm; the high-voltage probe had a voltage division ratio of 1000:1 and was used to measure the high-frequency sinusoidal experimental voltage; the high-speed digital oscilloscope had a maximum sampling rate of 5 GS/s and a sampling bandwidth of 1.5 GHz. During the test, the external UHF sensor was placed at 100 mm near the test chamber to collect the discharge signal mainly by detecting the electromagnetic wave propagating through the “gel-solid” insulation material. The sensor signal and the applied voltage signal were connected to the digital oscilloscope simultaneously, and the data collected in real time were transferred to the computer for storage and subsequent signal processing and statistical analysis through the USB serial bus and the data acquisition and storage system developed by LabVIEW.

FIGURE. 2.  Surface discharge test platform

The electrodes of the column and plate were made of brass according to the CIGRE Method Ⅱ standard; the ceramic substrate in the test was aluminum nitride of size 40 mm×40 mm×0.5 mm, the specimen was placed flat above the plate electrode, and the high-voltage column electrode was pressed against the upper surface of the specimen; the cavity was potted with the prepared silicone gel. Aluminum nitride and silicone gel samples were subjected to cleaning, preparation, deaeration and drying pretreatment before using.

In order to avoid the influence of dirt and moisture on the dielectric properties and experimental results of aluminum nitride, the specimens were cleaned with anhydrous ethanol and dried in an oven at 60 °C for 2 h. Before potting, the silicone gel needed to be prepared first. 50 g of A and B components were measured with an electronic balance, stirred well with a mechanical stirrer, and then injected into the cavity with fixed electrode and ceramic substrate, so that the silicone gel completely covered the electrode. Put into the vacuum drying oven, pumped under 0.1 MPa air pressure for 5 min, and then heated to 60 °C for curing for 4 h.

In this paper, at six different voltage frequencies of 5 kHz, 10 kHz, 15 kHz, 20 kHz, 25 kHz, and 30 kHz, the 100 V/s rapid boosting method was used to step up the voltage by until the partial discharge and surface flashover were formed, and the creeping partial discharge initial voltage and flashover voltage were recorded. Afterwards, the creeping partial discharge initial voltage and flashover voltage at different frequencies were compared to determine the voltage of the subsequent constant-voltage experiments, at which the pressure was continuously applied until the flashover occurred on the surface of the specimen. During the constant voltage experiment, the amplitude, number and phase of discharge pulses were recorded in real time by the discharge data acquisition system, and the development process of bubbles generated by the creeping discharge of “gel-solid” insulation was photographed at close range with a camera.

- 2.2 Surface morphology measurement

After the insulating material was discharged, the morphology of the discharged surface of the “gel-solid” insulating aluminum nitride ceramic substrate was analyzed by scanning electron microscopy (SEM, Hitachi S4800, Japan) at different stages of discharge damage.

- 2.3 Surface product measurement

The elemental content of insulating materials and changes in the structure of organic polymers were important indicators of creeping discharge, and structural changes in materials were analyzed by studying changes in the elemental content of materials and in the strength of functional groups using Fourier transform infrared spectrometry (FT-IR) and X-ray energy dispersive spectroscopy (EDS).

- 2.4 Surface conductivity measurement

The surface conductivity of aluminum nitride ceramic substrates at different damage stages was measured using a homemade three-electrode system with an ambient temperature of 20 °C, air humidity of 40 % ± 2 %, voltage DC of 1 kV, and 10 min electrolysis time. In order to make the measured values more accurate, the specimens were removed and measured five times, and the average of the measured values was taken as the surface conductivity of the ceramic substrate at this stage.

- Experimental results

- 3.1 Solid-liquid duality of silicone gel

The silicone gel was a special colloidal substance between solid and liquid, an elastic binder composed of silicon-oxygen links, whose side chains were connected with other organic groups by silicon atoms; therefore, there were components of both inorganic structures and organic groups in silicone gels [14]. Its chemical structure is shown in Fig. 3.

FIGURE. 3.  Molecular formula of silicone gel

The unique chemically cross-linked silicone polymer network structure of the silicone gel gave it strong elastic properties and retained the basic structural framework of silicone oil, but even at a high temperature of 200 °C, the silicone gel did not flow like a liquid. In solids, the cavities created by the discharge could exist for a long time, resulting in permanent defects; in liquids, the discharge was caused by flow injection consisting of high-temperature ionized gas cavities that disappear rapidly, usually within a period of time at atmospheric pressure, after the withdrawal of the applied voltage. And in silicone gel, we could get intermediate results that the discharge was also caused by flow injection consisting of high temperature ionized gas cavities (Fig. 4(a)), which was similar to liquid, and due to the liquid nature of silicone gel, its self-healing property enabled the generated gas cavities to slowly return to their original state, but in some severely damaged and discharged main channel locations, it formed permanent defects similar to solid (Fig. 4(b)).

(a) After discharge           (b) After self-healing

FIGURE. 4.  Solid-liquid duality of silicone gel.

- 3.2 Parameter statistics of “gel-solid” creeping discharge characteristics

- 3.2.1 Development process of creeping discharge

Firstly, the partial discharge initial voltage (PDIV) was determined in the pre-experiment by using the fast ramp-up method of 100V/s, each group of experiments was repeated five times, and the experimental results showed that the PDIV variation at each frequency and temperature was mainly concentrated around 5kV, and the experimental voltage to keep constant was 1.2-1.5 times of the PDIV [15], so the voltage in the constant voltage experiment was determined to be 7kV.

The development process of creeping discharge of silicone gel-aluminum nitride under high-frequency electrical stress is shown in Fig. 5 (take 20 ℃、10 kHz as an example). At the beginning of the discharge, the aluminum nitride insulation state was good, and the impurities and bubbles in the silicone gel were minimal in the initial stage after pretreatment, so it was not easy for the discharge to occur, but due to the high electric field strength at the triple junction point of the electrode, aluminum nitride and silicone gel, charged particles continuously impact the aluminum nitride surface under the action of the vertical component of the electric field, causing the local temperature to rise and promoting the decomposition of the silicone gel to form small bubbles, and at the same time, the a part of space charge would accumulate at the interface of aluminum nitride to promote the development of discharge, as shown in Fig. 5(a). After a long time of discharge, both silica gel and aluminum nitride were damaged to a certain extent, and many discharge channels in the form of bubbles were formed near the electrode due to the continuous bombardment of charged particles, and the discharge channels developed along the silicone gel-aluminum nitride interface, and a large number of bubbles could be observed to start to gather around the electrode at this stage, and the discharge started to develop steadily, as shown in Fig. 5(b). With the deep development of discharge, a large number of layered bubbles would be generated on the surface of aluminum nitride under the effect of strong local discharge, and larger bubbles started to form and extended continuously along the electric field line direction, as shown in Fig. 5(c), at this time, the insulation property of gel and aluminum nitride decreased rapidly due to the continuous bombardment of charged particles, which would eventually lead to surface flashover at the position of bubble penetration. After the silicone gel and AlN were peeled off, the obvious creepage marked on the surface of aluminum nitride could be observed in Fig. 5(d).

(a) Initial stage                            (b) Development stage

(c) Pre-flashover stage              (d) Creepage traces

FIGURE. 5.  Physical phenomena and insulating material conditions during discharge

3.2.2 Characteristic parameters of different stages of creeping discharge at each frequency

Triple junction point

In order to study the effect of frequency on the variation pattern of creeping discharge characteristics at different stages, 20 % of the insulation life along the surface at 5 kHz, 10 kHz, 15 kHz, 20 kHz, 25 kHz, and 30 kHz were taken as time nodes, and the development of creeping discharge was divided into five stages, and 300 typical circumferential discharge signals were taken between each two nodes, and the discharge characteristic parameters (maximum discharge amplitude and pulse repetition frequency) of each stage were counted, and the variation pattern is shown in Fig. 6.

(a) Maximum discharge amplitude

(b) Pulse repetition frequency

FIGURE. 6.  Statistics of surface discharge parameters at different stages at each frequency

The statistical results show that there is a “frequency-induced inflection point” in the growth of the maximum discharge amplitude and pulse repetition frequency throughout the discharge phase [16], with higher maximum discharge amplitude and pulse repetition frequency at 20 kHz compared to other frequencies. In the 0 - 80 % phase, the maximum discharge amplitude increases smoothly, whereas in the 80 % - 100 % phase, the maximum discharge amplitude increases rapidly at all frequencies. For the pulse repetition frequency of the discharge, the maximum value is reached at about 60% of the development level (with a maximum at the 80% position at 30 kHz). It is analyzed that the degree of discharge becomes more intense with the development of the discharge, so the maximum discharge amplitude shows a stage increase; when the discharge develops to the middle and late stages, the material damage becomes severe and the number of small-amplitude discharges decreases, leading to a decrease in the discharge pulse repetition frequency.

Based on the above-mentioned variation patterns of maximum discharge amplitude and pulse repetition frequency, it can be concluded that the three stages of development 0 - 40%, 40% - 80%, and 80% - 100% correspond to the initial stage, development stage, and pre-flashover stage, respectively. From the start of creeping discharge to 80% development, the maximum discharge amplitude increases at 5 kHz, 10 kHz, 15 kHz, 20 kHz, 25 kHz, and 30 kHz frequencies are 55.05%, 55.53%, 36.56%, 57.26%, 20.8%, and 20%, respectively, with the fastest increase in discharge amplitude at the inflection point frequency of 20 kHz; while the maximum discharge amplitude increases at 80% - 100% stage, the maximum discharge amplitude growth is 54.48%, 48%, 25.05%, 26.84%, 33.6%, 52.4%, and its growth rate is much larger than the first four small stages, so the surge of the maximum discharge amplitude can be used as a sign characteristic of the pre-flashover stage of the creeping discharge. Meanwhile, when the discharge enters the middle and late stages (after 60%-80% of development), the pulse repetition frequency will show a continuous decreasing trend, which can be used as an indicator to assess the severity of creeping discharge.

- 3.2.3 The effect of coupled temperature-frequency effects on the creeping discharge characteristics

In this paper, the characteristics of the creeping discharge under the coupled temperature-frequency effects were studied (frequencies of 5, 10, 15, 20, 25 and 30 kHz and temperatures of 20, 50, 80, 100 and 120°C). Fig. 7(a) shows the variation law of PDIV with temperature at different frequencies. From the figure, we saw that there was little relationship between the PDIV amplitude and the variation of the frequency of the applied voltage, and we believed that the onset voltage of the “gel-solid” creeping discharge was independent of the frequency magnitude, which was similar to the results reported in the literature [17-18]. And comparing the experimental results of each frequency at different temperatures showed that the PDIV decreased gradually with the increase of temperature. The average amplitude of PDIV decreased by about 35 % when the experimental temperature increased from 20 °C to 120 °C. The maximum discharge amplitude and pulse repetition frequency at different temperatures at different frequencies were further calculated, and the results are shown in Fig. 7(b) and (c), which show that the maximum discharge amplitude and pulse repetition frequency increase significantly with increasing temperature, independent of the frequency. The maximum discharge amplitude and pulse repetition frequency increase and then decrease with the increase of frequency at the same temperature, and the "frequency-induced inflection point" is 20 kHz. The minimum differences between the maximum discharge amplitude at 20 kHz and the maximum discharge amplitude at its adjacent frequency are 8mV, -3.3mV, 5mV, 7.8mV and 4.6mV, respectively, while the minimum differences between the pulse repetition frequency at 20 kHz and its adjacent frequency are 8.3×106 times/s, 1.06×106 times/s, 4.83×106 times/s, 0.72×106 times/s and 3.13×106 times/s, respectively. It can be seen that the increase in temperature has a certain weakening effect on the "frequency-induced inflection point" phenomenon, because when the high-frequency thermogenic effect gradually saturates, the increase in temperature increases the insulation surface and body conductivity, which further promotes the space charge dissipation and weakens the inhibition of the discharge by the space charge accumulation.

(a) Discharge starting voltage along the surface

(b) Maximum discharge amplitude

(c) Pulse repetition frequency

FIGURE. 7.  Statistics of discharge parameters along the “gel-solid” surface under coupled temperature-frequency effects

- 3.3 The surface damage characteristics of the ceramic substrate

The local high temperature and violent particle motion generated by the discharge were the main causes of surface damage of the material. In this paper, the surface morphology of aluminum nitride ceramic substrates at different damage stages was analyzed by scanning electron microscopy, and FT-IR spectroscopy and EDS tests were used to study the elemental content and structural changes of organic polymers.

As shown in Fig. 8, the aluminum nitride ceramic substrate made from high temperature sintered powder before discharge treatment was porous with a large number of irregular bumps and cavities. The results of infrared spectroscopy measurements and literature [19-20] tests suggested that the -N=N= double bond stretching vibration peaks were typical of the functional group characterization of aluminum nitride ceramic substrates. With the occurrence of discharge, the bumps on the surface of the substrate in the first stage gradually disappeared due to the arc “ablation”, and only the larger bumps remained, and the overall surface was smooth and flat; in the second stage, the ceramic substrate surface was continuously “eroded” by the longer time discharge, resulting in a large number of irregular granular solids on the substrate surface. A large number of irregular granular solids appeared on the surface of the substrate, with an obvious sense of concavity and convexity; the third stage of the substrate surface there were a large number of “craters”, the distribution of granular solids was more dense, the surface of large particles was often attached to a certain number of small particles, showing a multi-layer morphological structure. In the fourth stage, the surface of the “karst cave” was smooth, but near the edge of the “karst cave”, there was a flocculent distribution of particle groups; in the fifth stage, the surface of the substrate has formed a more obvious discharge channel, with the more obvious “bubble” phenomenon on both sides, at the same time there were “cracks”. The FT-IR spectra of the substrates in each discharge stage showed that the main spectral regions of the newly added absorption peaks were mainly the Si-O-Si bond stretching vibration peaks and the Si(-CH3)2 group in the main chain of the silicone gel, but there were also new CH out-of-plane bending vibration peaks in the -CHO group, O-N single bond stretching vibration peaks in the O-N=O group and NH2 out-of-plane wobble vibration peaks. The EDS test revealed that the elemental content of N and Al on the surface of the ceramic substrate decreased and the elemental content of C, O, and Si increased after the discharge (Fig. 9). The comprehensive analysis concluded that the discharge process was accompanied by the desorption of nitrogen and the generation of aluminum on the surface of the ceramic substrate, and the desorbed nitrogen was involved in the chemosynthesis reaction to generate amino compounds and nitrous compounds; whereas the generation of bending vibrational peaks outside the CH surface in the -CHO group indicated that the silicone gel underwent cross-linking reactions at high temperatures to generate aldehydes dominated by formaldehyde. Similar results were obtained in the literature [7, 21] in the study of cross-linking degree of the silicone gels and oxidation of aluminum nitride substrates.

FIGURE. 8.  SEM diagram and FT-IR spectrum of ceramic substrate at different discharge stages

FIGURE. 9.  The content of major elements on the surface of the ceramic substrate before and after discharge

As shown in Fig. 10, the surface conductivity of ceramic substrates generally tended to increase at different frequencies at various discharge stages. The analysis showed that the surface conductivity of the sample without discharge treatment to the first stage was slightly increased, mainly because the “ablation” process polishes the surface of the original sample with smooth bumps and shortens the surface creep path; the surface conductivity of the second stage started to gradually increase, which was mainly due to the fusion and aggregation of water and nitrite compounds on the surface of the second stage discharge. In the third stage, the surface conductivity showed an obvious rising trend, mainly due to the desorption of nitrogen caused by the discharge and the partial conversion of aluminum nitride into aluminum; in the fourth and fifth stages, the rising rate of surface conductivity slowed down, mainly because the oxygen element from the cleavage of silicone gel caused the oxidation of aluminum nitride substrate surface to generate aluminum oxide, which inhibited the degradation of surface discharge, thus led to the slowing down and eventual stabilization of the rising rate of surface conductivity.

FIGURE. 10.  The surface conductivity of the ceramic substrate changes periodically with discharge

- Results analysis and discussion

- 4.1 Evolution characteristics of “gel-solid” creeping discharge

- 4.1.1 Theoretical analysis of the evolution of the “gel-solid” creeping discharge process

“Gel-solid” insulation creeping discharge was a flow injection development process mainly characterized by bubble expansion and internal collisional ionization, in which the gel phase change (vaporization/cavitation) was the key process affecting the initiation and development of creeping discharge under high-frequency electrical stress. In silicone gel, the strong electric field led to an increased dissociation of colloidal molecules, which enhanced the electrical conductivity in the strong field region, while the Joule heat generated heated the colloid to vaporize it and promoted the formation of bubbles. The bubbles provided a site for the collisional ionization of internal gas molecules and were one of the fundamental processes in the formation of flow injection discharge in the gel.

When gaseous dielectric bubbles appeared in a homogeneous colloidal dielectric space, the dielectric bubbles were subjected to electric field forces due to the inhomogeneity of the electric field [22]. In this paper, the model of the electric field force on the bubbles generated during the creeping discharge of the silicone gel-AlN was as follows:

(1)

In the formula: r is the bubble radius; εrs and εrg are the relative dielectric constants of silicone gel and silicone gel vapor, respectively. In which, εrg can be considered as 1 like other gas dielectric constants.

Under the action of electric field, field ionization and collisional ionization were the main ways to produce charged particles. The probability of an electron leaping to a higher energy level to become a free electron under the action of an electric field in Zener's theory [23] could be expressed as:

(2)

Based on the electron tunneling theory [24], the field ionization charge density was introduced as:

(3)

In the formula: q is the charge, N is the number density of colloid molecules, a is the molecular spacing, m is the effective electron mass, h is Planck's constant, E is the externally applied electric field strength, Δ is the ionization potential.

A large number of space charges move directionally under the electric field to form a current, which led to an increase in the temperature of the colloidal dielectric through the Joule heating effect. When the temperature of the colloid at the triple junction point was greater than the saturated vapor temperature at this pressure, a unique physical phenomenon of “cavitation” [25] occurred. Due to the continuous heating of the electric field, accompanied by the formation of plasma, the heating inside the bubble and the evaporation of the colloid, the bubble expanded rapidly along the electric field lines. When the gas density inside the bubble was less than the critical value, the electrons were able to obtain high enough energy between two collisions to cause collisional ionization of colloidal molecules, which in turn formed an electron avalanche process that promoted the further development of the flow injection channel and eventually formed a creeping flash inside the bubble at the colloidal-solid interface. The discharge development process is shown in Fig. 11.

FIGURE. 11.  The development process of gel - solid surface discharge

- 4.1.2 Influence mechanism of bubble and air gap on the characteristics of the “gel-solid” creeping discharge

In the experiments, we noticed that the vacuum treatment helped to reduce the “gel-solid” creeping discharge activity, based on which the effect of the sample's own properties on the discharge was studied. In this paper, the degassing during the preparation of silicone gel-AlN was divided into three cases: 1) complete non-degassing; 2) semi-degassing, that is, the silicone gel was degassed and then potted with AlN; 3) complete degassing, that is, the silicone gel was degassed first and then potted with AlN and then jointly degassed.

We found that the partial discharge initial voltage of the samples treated with complete degassing during the preparation process was reduced by about 30% compared with that of the non-degassed samples. In addition, the severity of discharge was significantly lower for the samples treated with vacuum degassing than for the non-degassing samples. The statistics of the discharge parameters for the non-degassing, semi-degassed and fully degassed samples are shown in Fig. 12. The un-degassed silicone gel-AlN interface was filled with a large number of bubbles, and since the gas medium strength and relative dielectric constant inside the bubble were smaller than those of the external colloid, the discharge inside the bubble was easier and more violent. The number and amplitude of discharge of the fully degassed samples were lower than those of the semi-degassed treated samples, mainly due to the porous nature of the aluminum nitride ceramic substrate made of high-temperature sintered powder, and SEM observations showed that the shape of the outer surface of the samples was very irregular due to the granular structure of AlN (Fig. 13), and the fully degassed silicone gel filled the air gap existing on the surface of the ceramic substrate, resulting in a weaker degree of discharge present at the “gel-solid” interface.

FIGURE. 12.  Influence of degassing mode on surface discharge characteristics

FIGURE. 13.  Image of the AlN surface observed by scanning electron microscopy

- 4.2 The influence mechanism of coupled temperature-frequency effects on the “gel-solid” creeping discharge

- 4.2.1 Effect of frequency on the characteristics of the “gel-solid” creeping discharge

Under the “gel-solid” insulation structure, the discharge mainly occurred in the bubble generated by high temperature ionization between the silicone gel and aluminum nitride. From the streamer theory, we knew that two conditions need to be satisfied to generate the discharge under high frequency electrical stress: 1) the field strength in the bubble exceeded the initial discharge field strength; 2) the initial electrons appeared to excite the electron avalanche.

The surface charge generated by the discharge created a charge accumulation on the insulating surface, which had an impact on the subsequent discharge process. The initial electrons were mainly generated by the surface charge, and the generation probability λ could be estimated by the Schottky-Richardson model [26].

(4)

In the formula, NSC(t) is the number of charges that can be decoupled from the dielectric surface at time t; , E, 0, e, 0, K, and T denote the decoupling function, instantaneous electric field strength, photoionization constant, fundamental charge, vacuum dielectric constant, Boltzmann constant, and absolute temperature, respectively.

For spherical bubbles at the “gel-solid” interface, the initial electron production probability decreased with the increase of the trapping work function. In addition, the increase in trap density helped to increase the number of discharges; the increase in trap energy level led to an increase in the discharge amplitude [16]. With the development of creeping discharge, the trap density and energy level increased, and the number and amplitude of discharges at each frequency continued to grow, but the bubble area increased to a certain level and then stopped changing, and the trap density basically stopped increasing. At lower frequencies, the high-frequency thermogenic effect played a major role, and the temperature rise led to a rapid decrease in the insulation properties of the material, which was conducive to the generation of traps and the increase in the trap energy level, resulting in an increase in the number and amplitude of discharges; whereas at higher frequencies, the high-frequency thermogenic effect gradually saturated the space charge dissipation time decreased, which increased the accumulation of space charge and inhibited the occurrence of discharges. As a result, the phenomenon of “frequency-induced inflection point” mentioned above appeared in the experiment.

- 4.2.2 Effect of temperature on the characteristics of the “gel-solid” creeping discharge

Further investigation of the mechanism of temperature influence on the “gel-solid” creeping discharge led to the analysis conclusion that: the “gel-solid” interface was easy to accumulate space charge at low temperatures, which on the one hand reduced the field strength within the flow injection channel, and on the other hand also hindered the development of the electron collapse, thus inhibiting the discharge occurrence. With the increase of temperature, the charge dissipation at the “gel-solid” interface was accelerated, and the effect of charge accumulation on the electric field distortion and the synthetic electric field within the bubble of the “gel-solid” interface was weakened [27-28]. At the voltage polarity reversal, the electric field excited by the surface charge at the “gel-solid” interface was in the same direction as the externally applied electric field, which would increase the synthetic electric field inside the bubble, thus increased the discharge amplitude. In addition, the temperature rise would increase the charge injection rate of the insulating material, while the surface conductivity of the material increased with the temperature [29], so that the surface charge could diffuse faster at the “gel-solid” interface, reducing the time interval between two adjacent discharges, resulting in an increase in the number of discharges [30]. In addition, the higher the temperature, the more serious the damage effect caused by the discharge, the depth and density of the interface trap gradually increased, the number of charges that could be decoupled increased, and the amount of discharge charge increased significantly (Fig. 14), which eventually manifested itself as a surge in the discharge amplitude and the number of discharges.

FIGURE. 14.  Schematic diagram of charge distribution at the positive and negative polarity “gel-solid” interface

In this paper, 10 sets of experiments were done at 10 kHz frequency for different temperatures (20 °C, 50 °C, 80 °C, 100 °C, 120 °C) for observing the experimental phenomena at different temperatures. From the experimental statistics in Table 1, the surface conductivity of the ceramic substrate gradually increased with the increase of temperature. At 20 °C, the number of longitudinal breakdown of the “gel-solid” insulation discharge was much greater than that of the surface flashover, but the probability of surface flashover increased greatly as the temperature increased, and no longitudinal breakdown even occurred above 100 °C. From the temperature rise mechanism analyzed above, we knew that this was because as the temperature increased, the surface conductivity of aluminum nitride ceramic substrate increased, while the silicone gel was more likely to overheat and generate bubbles, compared to the aluminum nitride longitudinal breakdown, the “gel-solid” interface was more likely to form discharge channels and occurred surface flashover.

TABLE 1 Statistical table of surface discharge experimental phenomena at different temperatures

| Temperature (℃) | 20 | 50 | 80 | 100 | 120 |
| --- | --- | --- | --- | --- | --- |
| Surface conductivity (10-12S) | 2.3784 | 2.5596 | 2.8245 | 2.9602 | 3.1972 |
| Number of longitudinal breakdown (times) | 7 | 5 | 1 | 0 | 0 |
| Number of surface flashover (times) | 3 | 5 | 9 | 10 | 10 |

- 4.2.3 Effect of temperature-frequency synergy on the characteristics of the “gel-solid” creeping discharge

In Table 2, the discharge results under the action of coupled temperature-frequency effects and the state of the insulation material at room temperature resting for 8h are recorded and observed. We saw that at each temperature, the discharge severity of different frequency from high to low was 20 kHz, 30 kHz, 10 kHz, respectively, and the self-healing effect was the opposite, which was similar to the phenomenon of “frequency-induced inflection point”. Compared with the low temperature experimental phenomenon, the high temperature led to more intense discharge at the adhesive-solid interface and more serious insulation damage.

TABLE 2 Discharge damage and self-healing at different temperature - frequency

|  |  | Low temperature | High temperature |
| --- | --- | --- | --- |
| 10kHz | before self-healing |  |  |
|  | after self-healing |  |  |
| 20kHz | before self-healing |  |  |
|  | after self-healing |  |  |
| 30kHz | before self-healing |  |  |
|  | after self-healing |  |  |

In this paper, we believe that the influence mechanism of coupled temperature-frequency effects on the “gel-solid” creeping discharge: the increase in frequency made the space charge off into the trap more often, easy to form more hot electrons, the “gel-solid” interface by the hot electron impacts more frequently, the combined effect of polarization and thermal effects to strengthen. With the increase of voltage frequency, the loss caused by polarization increased, resulting in the rise of the internal temperature of the medium; at the same time, due to the capacitive properties of the insulating material, the higher the frequency, the greater the displacement current, which increased the power density of the electrode, and the impact of the high frequency strong displacement current increased the local heat production of the electrode, further promoting the increase of the number of discharges on the basis of the current temperature effect [31]. Based on coupled temperature-frequency effects, the increase in temperature had a greater degree of influence on the discharge characteristics of the insulating material, while the space charge effect caused by the change in frequency also had an extremely obvious effect on the discharge characteristics of the insulating material.

- 4.3 The influence mechanism of substrate damage on creeping discharge

According to the development of creeping discharge morphology and discharge characteristic parameters, took 20 ℃, 10 kHz as an example, the development process of creeping discharge under high-frequency electrical stress was divided into five stages according to the insulation life 20 %, and further divided into initial stage, development stage and pre-flashover stage according to experimental phenomena. whose PRPD spectra were shown in Fig. 15. The analysis of the material surface damage could be seen that it showed different change characteristics with the development of the discharge, while the discharge also became more intense with the deepening of the material surface damage. Therefore, it was considered that the discharge development pattern could be used to judge the surface condition of the material and the development of defects.

(a) Initial stage

(b) Development stage

(c) Pre-flashover stage

FIGURE. 15.  PRPD spectra at different stages

TABLE 3 Surface damage and discharge mode at different discharge stages

|  | Initial stage (1,2) | Development stage (3,4) | Pre-flashover stage (5) |
| --- | --- | --- | --- |
| Surface damage | ablation, erosion | karst cave, pit | bubbling, crack |
| Surface products | the content of N and Al elements decreased the content of C, O and Si elements increased |  |  |
| Surface conductivity | steady rise | significantly increase | stabilize |
| Discharge mode | overall lower, turtle back | the polarity reversal is high, the peak is low | layering proliferates, clustered |

As seen in Table 3, the first and second stages were the initial discharge stage, there was corona discharge at the “triple junction points”, at this time the material insulation performance was still good, the conductivity growth rate was slow, the discharge amplitude in the cycle was small, the discharge pattern showed the turtle back. The third and fourth stages were the development stage of flow injection along the surface, the plasma channel appeared inside the bubble of “gel-solid” insulation interface, the corona discharge developed to flow injection discharge, the surface of the material was seriously damaged at this stage, accompanied by the desorption of nitrogen and aluminum generation in aluminum nitride, the surface conductivity rose rapidly; at this time, the discharge amplitude near the peak basically remained unchanged, whereas more large value discharges appeared at the reversal of polarity, the number of discharges and discharge amplitude continuously increased. The fifth stage was the pre-flashover stage, in which the material surface was irreversibly damaged, the conductivity was larger and basically stabilizes, the discharge amplitude at the polarity reversal and near the voltage peak suddenly increased in a stratified manner at this stage, the plasma channel developed and extended toward the ground electrode, and finally the along-surface flow injection discharge through the gap appeared, forming the creeping flashover. Therefore, this paper considered that the “gel-solid” surface discharge pattern was mainly determined by the material damage characteristics.

- Conclusion

In this paper, we built a “gel-solid” creeping discharge test system of the power device package insulation of multi-energy conversion equipment. Firstly, the high-frequency creeping discharge characteristics of the silicone gel-aluminum nitride interface under the coupled temperature-frequency effects were statistically examined. Then, the evolution mechanism of the “gel-solid” insulation creeping discharge is analyzed based on the bubble theory, and the influence mechanism of the sample's own properties on the “gel-solid” insulation creeping discharge is investigated. Finally, the insulation discharge damage at the silicone gel-aluminum nitride interface is characterized, and the correlation between the coupled temperature-frequency effects and the substrate damage and the “gel-solid” creeping discharge is discussed. The following conclusions were obtained:

- Under the coupled temperature-frequency effects, the partial discharge initial voltage is independent of the frequency, but increases with the increase of temperature; the maximum discharge amplitude and the pulse repetition frequency gradually increase with the increase of temperature, whereas increase and then decrease with the increase of frequency, and the phenomenon of “frequency-induced inflection point” exists near 20 kHz; in addition, the study shows that the increase of temperature has a certain weakening effect on the phenomenon of “frequency-induced inflection point”.

- The SEM, FTIR spectroscopy and EDS analysis of different discharge stages showed that the “gel-solid” creeping discharge process was accompanied by the desorption of nitrogen and the generation of aluminum, and the production of aldehydes, nitrites and amino compounds, which was also the reason for the gradual increase and final stabilization of the surface conductivity.

- Based on bubble theory, material phase transitions and streamer theory, etc., the evolution mechanism of creeping discharge of “gel-solid” insulation is analyzed. And the influence mechanism of material own defects on the discharge is studied by changing the degassing method.

- The discussion concluded that the coupled temperature-frequency effects had a significant effect on the development of creeping discharge; the bubbles in the colloid and the air gap in the substrate were important factors affecting the discharge; and the creeping discharge pattern was mainly determined by the damage characteristics of the substrate.

- Acknowledgments

Financial support from the National Key R&D Program of China (2021YFB2601404) are here acknowledged.

- References

| [1] | Chen T, Zhang B B, Xu N, et al. Analysis of temperature cycling and insulation characteristics of highly reliable IGBT modules. Electronic Process Technology, 43(6), 320-323(2022) |
| --- | --- |
| [2] | Li W Y, Wang Y L, Yin Y. A review of reliability studies on packaging insulation of high-voltage power modules. Proceedings of the CSEE, 42(14), 5312-5326(2022) |
| [3] | YOU H Y, WEI Z, HU B X, et al. Partial discharge behaviors in power modules under square pulses with ultrafast dv/dt. IEEE Transactions on Power Electronics, 36(3), 2611-2620(2021) |
| [4] | T. Lebey, D. Malec, S. Dinculescu, et al. Partial discharges phenomenon in high voltage power modules. IEEE Transactions on Dielectrics and Electrical Insulation, 13(4), 810-819(2006) |
| [5] | SATO M, KUMADA A, HIDAKA K, et al. On the nature of surface discharges in silicone-gel: pre-breakdown discharges in cavities. IEEE Conference on Electrical Insulation and Dielectric Phenomena (CEIDP), Des Moines, USA, 19-22(2014) |
| [6] | SATO M, KUMADA A, HIDAKA K, et al. Dynamic potential distributions of surface discharge in silicone gel. IEEE Transactions on Dielectrics and Electrical Insulation, 22(3), 1733-1738(2015) |
| [7] | M. Sato, A. Kumada, K. Hidaka, et al. Surface discharges in silicone gel on AlN substrate. IEEE Transactions on Dielectrics and Electrical Insulation, 23(1), 494-500(2016) |
| [8] | J.-L. Auge, O. Lesaint and A. T. V. Thi. Partial discharges in ceramic substrates embedded in liquids and gels. IEEE Transactions on Dielectrics and Electrical Insulation, 20(1), 262-274(2013) |
| [9] | T. A. T. Vu, J. -L. Augé, O. Lesaint, et al. Partial discharges in Aluminium nitrite ceramic substrates. IEEE International Conference on Solid Dielectrics, 1-4(2010) |
| [10] | Fu P Y, Zhao Z B, Li X B, et al. Surface discharge characteristics and initiation mechanism of PEEK in nitrogen under semi-square voltage. AIP Advances, 8(7), 075322(2018) |
| [11] | Fu P Y, Zhao Z B, Li X B, et al. The role of time-lag in the surface discharge inception under positive repetitive pulse voltage. Physics of Plasmas, 25(9), 093518(2018) |
| [12] | Meng X R, Li X B, Li Y, et al. Influence of rise time and fall time on surface discharge characteristics of PEEK under positive repetitive square voltage. IEEE Transactions on Dielectrics and Electrical Insulation, 28(1), 183-191(2021) |
| [13] | Yang Z D, Li X B, Meng X R, et al. Influence of frequency on the surface discharge characteristics of PEEK under positive repetitive square voltage. High Voltage, 5, (6), 669-678(2020) |
| [14] | Oh J Y, Li X B, Cui X, et al. Preparation process and electrical resistance of silicone gel for high-voltage high-power IGBT device packaging. Journal of Electrical Engineering Technology, 36(2), 352-361(2021) |
| [15] | Liu Y, Dong M, Xing Y, et al. Development law and stage characteristics of multi-physical signals of surface discharge in oil-paper insulation. Proceedings of the CSEE, 43(4), 1611-1622(2023) |
| [16] | Liu T, Li Q M, Huang X W, et al. Frequency-inflection phenomenon and formation mechanism of partial discharge in polyimide films. Chinese Journal of Electrical Engineering, 37(9), 2750-2759(2017) |
| [17] | Ayubi, B.I, Zhang L, Xu H, et al. Surface discharge characteristics and influencing factors of polyimide insulations under high-frequency sinusoidal voltages. IET Generation Transmission & Distribution, 16, 1000-1012 (2022) |
| [18] | Gao B, Li Y, Liu K, et al. Charge migration of multilayer oil paper on the process of partial discharge under AC voltage. IET Generation Transmission & Distribution, 15, 2075-2084(2021) |
| [19] | Huang H J, Zhou H P, Wang Y D. Application of infrared spectroscopy in the testing of dispersion properties of AlN cast pastes. Journal of Inorganic Materials, 2002(2), 380-384(2002) |
| [20] | Liu F D, Liang Z N. Infrared absorption spectroscopy and Raman spectroscopy of aluminum nitride films. Journal of Optics, 1989(8), 752-757(1989) |
| [21] | Chen R R, Zeng F P, Su D Z, et al. Thermal aging characteristics analysis of silicone gel for high-voltage high-power IGBT packaging. Journal of Nanchang University (Science Edition), 46(2), 248-255(2022) |
| [22] | Cai D. Simulation study on the effect of air bubbles on the insulation performance of liquids. M.S. thesis, National University of Defense Technology, Changsha, China, 2011. |
| [23] | C. Zener. A theory of the electrical breakdown of solid dielectrics. Proc. Roy. Soc. A, 145(855), 523-529(1934) |
| [24] | O'SULLIVAN F M. A model for the initiation and propagation of electrical streamers in transformer oil and transformer oil based nanofluids. Ph.D. dissertation, Massachusetts Institute of Technology, Dept. of Electrical Engineering and Computer Science, Cambridge, USA, 2007. |
| [25] | Wu J, Zhang X D, Liu X W, et al. Hydraulic cavitation and applications. Chemical Industry and Engineering, 20(6), 387-391(2003) |
| [26] | A. Beroual, L. Kebbabi, E. Al-Ammar, et al. Analysis of creeping discharges activity at solid/liquid interfaces subjected to ac voltage. IET Generation Transmission & Distribution, 5, 973-978(2011) |
| [27] | Tao Y． Influence of temperature on partial discharge UHF characteristics of GIS defects．Beijing：North China Electric Power University(Beijing) , 2018． |
| [28] | Du B, Liang H, Li J, et al. Temperature dependent surface potential decay and flashover characteristics of epoxy/SiC composites. IEEE Transactions on Dielectrics and Electrical Insulation， 25(2), 631-638(2018) |
| [29] | Du B, Liang H, Li J, et al. Electrical field distribution along SG6/N2 filled DC-GIS/GIL epoxy spacer. IEEE Transactions on Dielectrics and Electrical Insulation， 25(4), 1202-1210(2018) |
| [30] | Li X, Xu Y, Ding D, et al. Influence of temperature on partial discharge and flashover characteristics of metal particle on GIS insulator surface. Proceedings of the CSEE, 42(1), 406-415(2022) |
| [31] | Han S, Li Q, Liu W, et al. Impacts of coupled temperature-frequency effects on partial discharge characteristics of high frequency solid state transformer insulation. Transactions of China Electrotechnical Society, 30(2), 204-210(2015) |