The new mathematical model approaches in biodiesel optimization

Volkan ASLAN*,

Department of Mechanical Engineering, Faculty of Engineering–Architecture, Yozgat Bozok University, 66200 Yozgat, Turkey

*Author e-mail: volkan.aslan@bozok.edu.tr

Abstract: Post-pandemic inflationist pressures, climate changes and extremes, regional conflicts, and soaring food prices caused the food crisis to increase rapidly worldwide. This global problem directs producers and researchers to use oils used as feedstock in biodiesel production effectively. In this context, it is important to assay the transesterification parameters and conduct new optimization studies to increase biodiesel yield. In this study, methyl ester was produced from hemp oil by transesterification using sodium hydroxide (NaOH). Next, classical optimization study was carried out to determine the effects of catalyst amount, alcohol:oil molar ratio, reaction temperature, and reaction time variables on biodiesel yield. Secondly, the cubic spline mathematical model (CSMM) and polynomial regression mathematical model (PRMM) was applied to the first data of this optimization. Among these optimization methods, the utmost biodiesel yield registered was 96.115% at hemp seed oil (HSO): methanol molar ratio of 5.59:1, catalyst concentration of 0.531 wt%, reaction temperature of 42.5 °C, reaction time of 62.1 min, and agitation intensity of 600 rpm at PRMM. Some vital fuel properties obtained from HSO biodiesels as a result of three optimizations satisfied the EN 14214 standard. The results illustrated that the optimal yields from CSMM and PRMM are 0.765% and 1.065% higher, respectively, according to the maximum efficiency obtained from the classical optimization. The outcomes showed that CSMM and PRMM are cost-effective, easy to handle and promising new approaches.

Key words: Hemp seed oil; Optimization; Fuel properties; Cubic spline mathematical method; Polynomial regression mathematical method

1. Introduction

Energy is used to meet human needs and enhance the quality of life, and it is one of the most important inputs that determine the economic and social development potential of a country.1 Nowadays, about 86% of the world's primary energy consumption is from fossil-based sources.2,3 However, humanity faces the hazard of depletion of fossil fuels.4 Moreover, it is seen that global climate change and ecological balance have deteriorated due to the greenhouse gases released into the air with the energy production from these fuels.5–7 Renewable fuels significantly minimize these disadvantages and reduce foreign-source dependency by using domestic resources.8 Biodiesel fuel is in demand owing to its convenient emission and combustion profile, carbon-neutral property, high flash point, and versatile usage. Although there are many methods to reduce the viscosity in crude oil to obtain biodiesel, transesterification is the most preferred method with its advantages (formation of products close to petrodiesel, commercialization potential, mild reaction conditions, renewability, cheap and high conversion, etc.).9,10 Transesterification is forming fatty ester and glycerine by reacting the triglyceride molecule with alcohol in the presence of a catalyst. Methanol and sodium hydroxide is the most chosen alcohol-catalyst binary in the transesterification reaction due to ease of handling, cheap and abundant availability, and high yield.11,12

The feedstock used in biodiesel production is selected considering many factors such as local availability, cost, quality, oil yield, fuel performance, renewability, origin, and government support. A wide variety of feedstocks can be evaluated in biodiesel production, such as vegetable (edible and inedible) oils, animal fats, waste oil, and algal oils.13,14 Approximately 95% of the feedstock used in biodiesel production is selected from edible oils. However, using these edible oils in biodiesel production has increased the interest in non-edible vegetable oils due to food safety, the gap between supply and demand, and their uneconomical nature.15,16

Hemp (Cannabis sativa L.) is one of the plants that accompanied humanity, dating back more than 8500 years.17 Industrial hemp is an agricultural product preferred in the production of a wide variety of products, including food and beverages, cosmetics and personal care products, nutritional supplements, fabrics and textiles, yarns and spun fibers, paper, construction and insulation materials, resin, pulp, animal bedding, fuel, etc.18,19 This plant is one of the fastest-growing biomass and aligns with the green future goals societies and governments aim to transition to in the 21st century. Also, it has wide adaptability and demands very few pesticides or herbicides.20

Hemp has a very developed root system that prevents soil erosion. The stem is green, straight, and blanketed with bristle. The edge of the lance-shaped leaf is jagged, and its surface is rough. The flowers are short prongs, without petioles, and are seated. The seeds vary in diameter depending on the cannabis variety, are egg-shaped, and are between 3 and 4 mm. The weight of the seed increases as it matures and is between 8-26 g. The color of the seed coat is mosaic and ranges from brown to dark gray. In practice, the most desirable seed is the one with a dark and bright hue.21 The root, stem, leaf, flower, and seed picture of the hemp plant (Cannabis sativa L.) is illustrated in Figure 1.

a

b

c

d

e

Figure 1. The pictures of hemp (Cannabis sativa L.). (a)-root, (b)-stem, (c)-leaf, (d)-flower, (e)-seed.21

According to 2021 data from the Food and Agriculture Organization (FAO), the production, area harvested, and yield of hemp seeds are around 5446-tonnes, 10566 ha, and 5155 hg/ha globally, respectively. For 2021, the country distributions of the annual production amount of hemp seed year were created with mapchart.net and are shown in Figure 2.

Figure 2. The country distributions of the annual production amount of hemp seed for 2021 year.22

Turkey, one of the world's cannabis producers, has recently increased its investment and support for hemp. The aim of Turkey's recent hemp policy is to produce and expand hemp production to meet the needs of many different fields. In this context, institutes were established for research and development in cannabis production, a new cannabis variety was developed, and an action plan was made with different ministries and organizations. Yozgat Bozok University, a university in Turkey, received approval from the government as a university specializing in the field of "Industrial Hemp" in 2020 and has started research and development works.

The catalyst type and dosage, free fatty acid and moisture content, alcohol type and quantity, reaction temperature, agitation speed, and reaction time have different degrees of influence on the integrity and efficacy of the transesterification reaction. It is essential to analyze the relations of these parameters and apply the proper optimization method from the point of product efficiency and cost.23,24 The parameters affecting the transesterification reaction are illustrated in Figure 3. Also, selecting the optimization method implemented to these parameters is essential. Classic, central composite design, Box-Behnken, and Taguchi are preferred methods.

Figure 3. The parameters affecting the transesterification reaction

Gupta et al. 25 evaluated the optimization of hemp (Cannabis sativa L.) oil transesterification variables using the Fresnel lens solar concentrator (FSC) approach and the conventional heating method approach. The reaction variables used are catalyst concentration (0.3-1.2%), alcohol: oil molar ratio (3:1-6:1), reaction time (10-80 min for conventional), and mixing speed (0-400 rpm). The yield of optimum cannabis oil methyl ester was obtained as 97.37% at 4 min reaction time, 4.5:1 methanol: oil molar ratio, 200 rpm mixing speed, and 0.90% catalyst concentration. Stamenković et al.26 investigated the optimization of hemp oil methanolysis production: catalyst amount (0.58-1.42 wt.% of the oil), methanol: oil molar ratio (3.5:1-8.5:1) and reaction temperature (23.2-56.8°C) and reaction time (up to 180 min). Biodiesel production process parameters were optimized using RSM and ANN combined with a genetic algorithm (GA). While the highest efficiency was 98.5% (predicted content: 99.8%) with the RSM method, it was determined as 97.5% (predicted content: 97.1%) with the ANN-GA method. Yilbasi and co-workers 27 appraised using the Taguchi method (applying an L9 orthogonal design matrix) for process optimization of reaction variables: KOH catalyst concentration (0.6–1.2%), methanol/oil molar ratio (6:1–12:1), reaction time (60–120 min), and reaction temperature (30–60°C). The optimal reaction conditions for achieving the highest FAME content (96.87%) in 120 min at the KOH loading of 0.9 (by the oil weight) was: the methanol-to-oil molar ratio of 12:1 and 45 °C reaction temperature. They also stated that the methanol oil molar ratio was the most influential factor, and the reaction time was the least effective parameter in this study. Finally, Rashid et al. 28 optimized process parameters in order to get maximum hemp seed oil (HSO) biodiesel using response surface methodology. The investigators optimized the methanol/oil molar ratio (varying from 3:1 to 9:1by steps of 1.5), NaOCH3 concentration (varying from 0.25 wt% to 1.50 wt% by steps of 0.31wt%), reaction temperature (varying from 45°C to 65°C by steps of 5°C), reaction time (varying from 30 to 90 min. of 15 min.). After all, the maximum Cannabis sativa oil biodiesel yield was determined by 86.01 % with 7.5:1 of methanol to oil molar ratio, 0.80 wt% of catalyst amount, 65 min. of reaction time, and 53°C of reaction temperature.

Nowadays, food supply security, irrigation shortage, necessary energy from planting to harvesting for seeds, climate change, etc. problems are increasing daily. Considering the feedstock problems, choosing a suitable optimization technique is important. A comparison of the classic method and mathematical models, that are cubic spline mathematical method and polynomial regression mathematical method, for optimizing transesterification of HSO biodiesel has not been informed up to now. Thus, the present study concentrates on optimizing the transesteriﬁcation of HSO for biodiesel production according to the classical optimization method by using the cubic spline mathematical method and polynomial regression mathematical method to analyze the optimal biodiesel production. At the same time, the current experimental study aims to analyze the impacts of the different process factors, including NaOH concentration, methanol:oil molar ratio, reaction temperature, and reaction time, on the conversion yield of HSO. Subsequently, the fatty acid composition and the elemental analysis of HSO biodiesel were identified. Finally, the physicochemical properties of the biodiesel fuels with the highest efficiency determined by three different optimization techniques were determined and compared by ASTM D6751 and EN14214.

Theoretical background

In this study, in addition to the classical method, the cubic spline mathematical method (CSMM) and polynomial regression mathematical method (PRMM) optimization of the transesteriﬁcation of HSO with methanol in the presence of NaOH were implemented in this work.

CSMM

A series of continuous curves bonded to compose a single continuous curve is named a spline curve. For (xj , yj), j = 0,1, ..., n – 1 and xj < xj+1, j = 0,1, ..., n considering a given set of data points; generally, m. degree spline f(x) for this dataset is a piecewise polynomial of degree m supplying the undermentioned two conditions: 29

- For each interval (xj, xj+1) için, it is at j = 0,1, ..., n – 1, ≤ m degree.

- At each node xi and in the range j = 1, ..., n − 1, (x0, xn); the spline f(x) and its first m -1 derivatives are continuous.

Cubic spline interpolation is finding a curve connecting data points with three degrees or less. Splines are uniform and continuous polynomials along a given graph and are also continuous first and second derivatives where they converge. In the cubic spline approximation, the approximate cubic polynomials, the function values are such that the first and second derivatives are continuous at the nodes. Therefore, the cubic spline curve is continuous, so the gradient and curvature remain the same everywhere in the whole area. For this reason, the cubic spline provides sufficient smoothness on the approximate curve. A cubic spline polynomial f(x) provides the following three conditions:30

- [xj-1, xj], 1≤ j ≤ n,  f(x) is a third-order polynomial at each subinterval.

fj(x)= ajx3+bjx²+cjx+dj               j=1,2,3,….,n

- Cubic spline values ​​at the nodes are equal to the numerical values ​​of the function at these points.

- The polynomials f'x,f ''x ve f'''x are continual along the interval. (xo, xn).

PRMM

The purpose of regression analysis is to estimate the parameters of the model established between the dependent variable and one or more independent variables and to determine the value of the dependent variable for the observed values of the independent variable.31 In some engineering calculations, the model formed by the data is unsuitable for a linear line. In such cases, using an appropriate curve for the data is necessary. At such times, the polynomial regression mathematical model is an evaluable method. The PRMM can be stated using Eqs. (1) and (2):

f(x)=a0+a1 x+a2 x2……….+amxm+e                                                                                       (1)

e=y-a0-a1 xi-a2 xi2……….-am xim                                                                                               (2)

where y, x, m,e, and a0,a1,..,am present dependent variable, independent variable, polynomial degree, error, and constant coefﬁcients, respectively.

2.3. Prediction of fuel properties

Biodiesel fuels with the highest biodiesel efficiency were obtained by determining the optimum values with each optimization method. The fatty acid compositions of these fuels were established via gas chromatography-mass spectrometry (GC-MS). Then, fuel properties of these biodiesels, such as density, kinematic viscosity, heating value, cetane number, flash point saponification number, iodine number, cloud point, cold filter plugging point, pour point, degree of unsaturation, oxidation stability were estimated using the fatty acid composition values by following equations (Table 1).

Experimental

Materials

Hemp (Cannabis sativa L.) seeds

The seeds of the ''Narlıdere'' type of Cannabis Sativa (Hemp seed), grown by the farmers of Yahyalı, a district of Turkey, were used. The HSO was obtained through a screw oil press

| Table 1. The equations used to predict fuel properties |  |  |
| --- | --- | --- |
| Property | Formula | Definitions |
| Density32 | ρi=0.8463+4.9Mi+0.0118⋅N | ρi :Density of ith fatty acid methyl ester (FAME) at 20°C Mi : Molecular weight of ith FAME N :Number of double bonds of given FAME |
| Kinematic viscosity32 | ln(ηi)=-12.503+2.496⋅ln(Mi)-0.178⋅N | ηi :Kinematic viscosity of ith FAME at 40°C |
| Heating value32 | δi=46.19-1794Mi-0.21⋅N | δi :Heating value of ith FAME |
| Cetane number32 | ϕi=-7.8+0.302⋅Mi-20⋅N | ϕi :Cetane number of ith FAME |
| Flash point33 | FP=32.641⋅η+305.02 | FP:Flash point |
| Saponification number34 | SN=i=1 n 560⋅AiMi | SN:Saponification number Ai :The percentage of each component in the fatty acid composition |
| Iodine value34 | IV=i=1 n 254∙N⋅AiMi | IV :Iodine value |
| Cloud point35 | CP = 0.526(C16:0)-4.992 | CP :Cloud point C16:0 :Percentage of palmitic acid |
| Cold filter plugging point36 | CFPP = 3.1417(LCSF)-16.477 LCSF = 0.1(16:0%)+0.5(C18:0%)+ +1(20:0%)+1.5(22:0%)+2(24:0%) | CFPP :Cold filter plugging point LCSF :Long chain saturated factor |
| Pour point37 | PP = -30.324+0.667(16:0%)+ +0.4065(18:0%)+0.11791(18:1%)+ +0.23225(18:2%)+0.17162(18:3%)+ -0.48149(22:1%) | PP :Pour point |
| Degree of unsaturation34 | DU = ∑MUFA+2∙∑PUFA | DU : Degree of unsaturation MUFA : Monounsaturated fatty acid PUFA : Polyunsaturated fatty acid |
| Oxidation stability38 | OS =[(16:1%+18:1%+20:1%+22:1%)+10.3x18:2%+21.6x(18:3%)]/100 | OS : Oxidation stability |

machine using 8 mm nozzles. Moisture and oil contents of the seeds were determined 5.12 ± 0.11 g/100 g and 25.19 ± 0.22 g/100 g, respectively. HSO was left to rest for a few days and was filtered with Whatman filter paper for the suspended oil cake particles to settle to the bottom. Before starting the optimization studies, the titration method designated the free fatty acid content of HSO. Since the average FFA value (% 0.384) of hemp oil is less than 1%, a one-stage homogeneous catalyst transesterification process was applied in the optimization studies. The average molecular weight of HSO was calculated from the distribution of fatty acid compositions with the Shimadzu single quadrupole GC-MS-QP2010 gas chromatograph-mass spectrometer.

Chemicals and devices

Methanol (99.8%) and NaOH (pellets pure) were procured from Merck (USA). KOH solution (0.1 N) and phenolphthalein indicator (% 1) were procured from Norateks Chemical Company (Turkey), and diethyl ether was bought from Tekkim Chemical Company (Turkey). The important device of the study IKA C-MAG HS 7 (Germany) package magnetic stirrer, runs at speeds ranging from 100-1500 rpm, a heating temperature range ranging from 20-500°C, temperature step of 0.1°C was used. The weight measurements of the samples were made with a Weightlab LB.WL-603 (Turkey) precision balance has a readability of 0.001 g and a weighing range of up to 600 g.

Transesterification of HSO

Apparatus and experimental method

Each trial was carried out with 100 g ± 0.01 of HSO in optimization studies. First, the weighed and noted HSO was poured into a three-neck flat bottom as shown in Figure 4. Afterwards, the desired reaction temperature was adjusted, the thermometer was mounted on the magnetic stirrer with heater, and the heating and mixing processes were started.

Figure 4. Experimental apparatus for transesteriﬁcation of HSO

Methanol and NaOH mixed in specific proportions were mixed in a glass container until NaOH dissolved. When the HSO reached the set temperature, the methanol-NaOH solution was spilled from one neck, and the time was started. The mixing intensity was fixed to 600 rpm for each trial. When the reaction time was complete, the mixture was transferred to a separatory funnel and left to rest for at least 8 hours to allow the glycerol to settle to the bottom. The ester was kept in the heater for 1 hour without stirring, at a temperature of 70 °C (due to the boiling point of methanol) to evaporate unreacted methanol. Then, the ester separated from glycerol was purified with distilled water. Ester and distilled water temperatures were chosen to be close to each other, between 50-55 °C. After purification, the wastewater was taken after waiting at least 8 hours. As a final process, the drying process was realized at 120 °C for 2 hours to remove the water in the ester. Some images related to HSO biodiesel production are presented in Figure 5.

a

d

c

b

Figure 5. Some images related to HSO biodiesel production; (a) ester and glycerol separation, (b) alcohol evaporation, (c) purification, (d) drying

The biodiesel yield at room temperature was calculated according to Eq. (3).39 The experimental procedure is depicted in Figure 6.

Biyodizel yield (%)=Amount of biodiesel produced (g)Amount of oil used (g)*100                                                       (3)

Figure 6. The experimental procedure for obtaining HSO biodiesel and calculating yield

Optimization of production parameters

Optimization processes were carried out to reach the maximum ester yield with the help of CSMM and PRMM. Methanol was selected as the alcohol and NaOH was chosen as the catalyst in optimization studies. The parameters examined using the transesterification method were catalyst concentration, methanol: HSO molar ratio, reaction temperature, and reaction time. Many researchers emphasized that examining these parameters affects transesterification.40–43 The parameter data for the optimization processes in this study are illustrated in Table 2.

Table 2. The optimization parameters and their numerical values

Optimization processes were started with the catalyst parameter variable and the other parameters fixed. The catalyst concentration varied from 0.4% by weight to 1.0% in 0.2% steps, while the molar ratio, reaction temperature, and reaction time were fixed at 5:1, 60°C, and 60 min., respectively. In the classical method, the catalyst concentration with the highest efficiency was selected in the biodiesel yields obtained depending on the catalyst concentration change. This value is taken as constant in other transesterification parameter processes. The CSMM approach, CSMM was applied using the biodiesel yields obtained from each parameter and the numerical variables determined for the relevant parameter. The value obtained with the CSMM application was fixed in other transesterification parameter processes. The PRMM approach pursued a similar tack to CSMM. PRMM and CSMM approaches aim to increase biodiesel production efficiency according to the classical optimization method. The flowchart relevant to using the optimization methods is illustrated in Figure 7.

Result and discussion

Fatty acid composition

The fatty acid composition of HSO was analyzed by gas chromatography-mass spectrometry (GC-MS) in Yozgat Bozok University Central Laboratory to determine the molecular weight required for the methanol: HSO molar ratio. At the end of each optimization study, biodiesels with the highest yield were produced, and GC-MS determined their fatty acid distributions. The fatty acid compositions of HSO and biodiesels (obtained from classical, CSMM, and PRMM) are shown in Table 3.

The dominant fatty acids in biodiesel produced in three optimization techniques are linoleic acid, oleic acid, and linolenic acid, similar to hemp oil, as shown in Table 2. According to the fatty acid composition, the average molecular weights of the biodiesels obtained by classical, CSMM and PRMM were calculated as 876.10, 875.98, and 876.07 g/mol, respectively.

Figure 7. Flowchart on the use of the optimization methods

| Table 3. The fatty acid compositions of HSO and biodiesel fuels |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| No | Fatty acid | Molecular weight | Structure | Formula | HSO | Classical | CSMM | PRMM |
| 1 | Palmitic | 256 | 16:0 | C16H32O2 | 7.18 | 7.84 | 7.54 | 7.80 |
| 2 | Palmitoleic | 254 | 16:1 | C16H30O2 | 0.06 | 0.07 | 0.07 | 0.06 |
| 3 | Margaric | 270 | 17:0 | C17H34O2 | 0.04 | 0.03 | - | 0.90 |
| 4 | Stearic | 284 | 18:0 | C18H36O2 | 3.21 | 3.72 | 3.89 | 3.69 |
| 5 | Oleic | 282 | 18:1 | C18H34O2 | 18.23 | 19.37 | 19.40 | 19.25 |
| 6 | Linoleic | 280 | 18:2 | C18H32O2 | 53.75 | 51.64 | 51.78 | 51.16 |
| 7 | Linolenic | 278 | 18:3 | C18H32O2 | 16.55 | 16.09 | 16.10 | 15.74 |
| 8 | Stearidonic | 290 | 19:4 | C18H28O2 | 0.22 | 0.22 | 0.19 | 0.21 |
| 9 | Arachidic | 312 | 20:0 | C20H40O2 | 0.41 | 0.46 | 0.47 | 0.49 |
| 10 | Behenic | 340 | 22:0 | C22H44O2 | 0.33 | 0.43 | 0.45 | 0.42 |
| 11 | Lignoceric | 368 | 24:0 | C24H48O2 | 0.25 | 0.14 | 0.12 | 0.27 |
|  | ΣSFA |  |  |  | 11.42 | 12.62 | 12.47 | 13.57 |
|  | ΣMUFA |  |  |  | 18.29 | 19.44 | 19.47 | 19.31 |
|  | ΣPUFA |  |  |  | 70.51 | 67.95 | 68.07 | 67.11 |

Optimization of HSO biodiesel production

The experiments were conducted with three different optimization techniques: Classical, CSMM, and PRMM. The transesteriﬁcation process was optimized using four parameters: catalyst concentration (0.4–1.0 wt%), methanol: HSO molar ratio(3:1–9:1), reaction temperature (30–60°C), and reaction time (30–75 min.).

Effect of catalyst concentration

The transesterification of the HSO to biodiesel was investigated under various catalyst concentrations, 0.4%–1.0%, at an interval of 0.2%, while other conditions were kept fixed: 5:1 molar ratio (methanol: HSO), 60 °C reaction temperature, 60 min reaction time and stirring at 600 rpm. The effect of catalyst concentration for different optimization conditions is given in Figure 8. As a result of the experiments, the highest yield was obtained with 94.95% at 0.6 catalyst concentration. These data were used in the classical method in the following reaction condition. The cubic spline mathematical model and polynomial regression mathematical model were applied to the catalyst concentration and biodiesel yield data. The highest yields and catalyst concentrations were determined at 95.05%–0.566 wt% and 95.28%–0.531 for CSMM and PRMM, respectively.

Figure 8. Effect of catalyst concentration on biodiesel yield for Classical, CSMM and PRMM methods.

It has been determined that the catalysts used at both high and low ratios reduce the efficiency, but there is an optimum point in the middle points. When a large catalyst dosage is utilized, the catalyst reacts with free fatty acids in the oil and form saponification. Conversely, when a low amount of catalyst is preferred, the reaction cannot be completed, and the ester is not formed.44 From Figure 8, it can be understood that the CSMM and PRMM applications increased biodiesel yield according to classical methods.

Effect of methanol:HSO molar ratio

The alcohol: oil molar ratio is one of the most critical reaction parameters affecting biodiesel yield. Although there is a 3:1 stoichiometric ratio between the oil and alcohol in the transesterification reaction, more stoichiometric ratios are needed to improve the mass transfer between the triglyceride and the alcohol molecule and to increase miscibility.45 Methanol: HSO molar ratios of 3:1, 5:1, 7:1 and 9:1 were studied using 60 °C and 60 min stirring at 600 rpm. Concentrations of catalyst were determined in the previous parameter study. In the classical method, the catalyst concentration corresponding to the highest efficiency was chosen as 0.6 wt%. Catalyst concentrations in CSMM and PRMM applications were established as 0.566 wt% and 0.531 wt%, respectively, with the aid of the applied equations. The influence of methanol: HSO molar ratio for different optimization conditions is shown in Figure 9.

Figure 9. Effect of methanol:HSO molar ratio for Classical, CSMM and PRMM methods on biodiesel yield.

The optimum yields and molar ratios were obtained at 94.95%–5:1, 95.20%–5.65:1, and 95.39%–5.59:1 for classical, CSMM, and PRMM, respectively. In each optimization study, it was concluded that the biodiesel yield decreased at high molar ratios. This decrease in yield may be due to the dissolution of glycerine in excess alcohol. It is not easy to separate the dissolved glycerin from the product.46

Effect of reaction temperature

The transesterification process can take place at different temperatures. The reaction temperature plays an active role in reaction rate and biodiesel yield.47 The reaction temperature used for the study was 30, 40, 50, and 60 °C, keeping the reaction time of 60 min. and agitation intensity of 600 rpm fixed. Catalyst concentrations and methanol: HSO molar ratios corresponding to the highest yield in the previous conditions were retained. For Classical, CSMM, and PRMM, the catalyst concentration was 0.6, 0.566, and 0.531 wt.%, respectively; the molar ratios of methanol: HSO were chosen as 5:1, 5:65, and 5:59, respectively. The effect of reaction temperature for various optimization conditions is given in Figure 10.

Figure 10. Effect of reaction temperature on biodiesel yield for Classical, CSMM and PRMM methods.

A decrease in temperatures below and above 40°C occurred. The optimum yields and reaction temperatures were attained at 95.05%–40°C, 95.80%–43.5°C, and 96.09%–42.5°C for classical, CSMM, and PRMM, respectively.

Effect of reaction time

The methyl ester yield increases as the reaction time increase to a certain point (optimum point). The reaction time beyond this point does not increase the conversion rate due to supporting the back reaction (hydrolysis of esters).48 Aslan and Eryilmaz49 stated that one hour might be appropriate for the optimal reaction time for the ester conversion. The values at the optimum points determined in the previous stages were used as the data of other parameters except for the reaction time. For Classical, CSMM, and PRMM, the catalyst concentration was 0.6, 0.566, and 0.531, respectively; the molar ratios of methanol: HSO were chosen as 5:1, 5:65, and 5:59, respectively; the reaction temperature was taken 40, 43.5, 42.5°C, respectively. The influence of reaction time for classical, CSMM, and PRMM is given in Figure 11. The yields peaked at around 60 min and then started to decline. The highest yields and reaction times were determined at 95.05%–60 min., 95.815%–63.4 min., and 96.115%–62.1 min. for classical, CSMM, and PRMM, respectively.

Figure 11. Effect of reaction time for Classical, CSMM, and PRMM methods on biodiesel yield.

Optimum transesterification parameter conditions and characterization of biodiesels

The optimal conditions for obtaining the maximum yield for each optimization as a result of three different optimization processes are given in Table 4. When the results are examined, the data obtained from the classical method are compatible with the results of a previously reported study in the literature.50 While the highest efficiency is obtained with the PRMM method at 1.065 % compared to the classical method, this increase is 0.765% in the CSMM method.

| Table 4. Optimum reaction conditions of Classical, CSMM, and PRMM methods |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Methods | Optimal condition variables |  |  |  |  |  |  |
|  | Catalyst Concentration (wt%) | Methanol:HSO molar ratio |  | Reaction Temperature (°C) |  | Reaction Time (min) | Yield (%) |
| Classical | 0.600 | 5.00:1 | 40.0 |  | 60.0 |  | 95.050 |
| CSMM | 0.566 | 5.65:1 | 43.5 |  | 63.4 |  | 95.815 |
| PRMM | 0.531 | 5.59:1 | 42.5 |  | 62.1 |  | 96.115 |

The HSO biodiesel produced by the transesteriﬁcation reaction was characterized to determine its physicochemical properties such as density, kinematic viscosity, calorific value, cetane number, saponification number, iodine number, flash point, cloud point, cold filter plugging point, pour point, unsaturation degree, and oxidation stability and shown in Table 5. According to the fatty acid compositions given in Table 3, the fuel properties of biodiesels were estimated with the aid of the equations given in Section 2.3.

| Table 5. The fuel properties of biodiesels derived from Classical, CSMM and PRMM methods |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | EN 14214 |  |  |  |  |
| No | Property | Unit | Min. | Max. | Classical | CSMM | PRMM |
| 1 | Density at 20°C | kg/m3 | 860 | 900 | 876.10 | 875.98 | 883.80 |
| 2 | Kinematic viscosity at 40°C | mm2/s | 3.5 | 5.0 | 3.48 | 3.48 | 3.49 |
| 3 | Calorific value | MJ/kg | - | - | 39.405 | 39.402 | 39.402 |
| 4 | Flash point | °C | 101 | - | 145 | 145 | 146 |
| 5 | Acid value | mg KOH/g | - | 0.50 | 0.82 | 0.98 | 0.79 |
| 6 | Cetane number | - | 51 | - | 38.435 | 38.600 | 38.888 |
| 7 | Iodine value | g I2/100 g | - | 120 | 155.82 | 155.09 | 155.84 |
| 8 | Saponification value | mg KOH/g | - | - | 200.69 | 200.68 | 200.64 |
| 9 | Polyunsaturated methyl ester (≥4 double bonds) | % (m/m) | - | 1 | 0.22 | 0.19 | 0.21 |
| 10 | Degree of unsaturation5 | - | - | - | 154.9 | 154.43 | 153.11 |
| 11 | Oxidation stability value, COX | h | - | >6 | 8.99 | 8.94 | 8.86 |
| 12 | Cloud Point, CP | °C | Report |  | -0.80 | -0.80 | -0.88 |
| 13 | Pour Point, PP | °C | - | - | -7.76 | -7.69 | -7.79 |
| 14 | Cold filter plugging point, CFPP | °C | Report |  | -3.82 | -3.76 | -3.84 |
| 15 | Alkali content (Na+K) | mg/kg | - | 5.0 | 0.541 | 1.378 | 1.121 |
| 16 | Alkaline-earth content (Ca+Mg) | mg/kg | - | 5.0 | 9.647 | 6.758 | 6.870 |
| 17 | Phosphorus content | mg/kg | - | 4.0 | n.d | n.d | n.d |

Table 5 presents that iodine number, acid number, and alkaline-earth content values are higher than the upper limit of the standard value. On the contrary, the cetane number values are lower than the sublimit of the standard value. The higher the number of double bonds, the higher the iodine number. The iodine number is also related to the cetane number. High unsaturation causes the decrease of cetane number in biodiesel.51

Conclusion

This work optimizes the condition variables using classical, CSMM, and PRMM methods. Optimization of transesteriﬁcation of the reaction of hemp seed oil was acquired by four parameters and four levels. The results show that parameters except reaction time have an important effect on biodiesel yield. The maximum biodiesel yield of 96.115% was achieved with NaOH concentration (0.531 wt%), HSO: methanol molar ratio (5.59:1), reaction temperature (42.5 °C), and reaction time (62.1 min) using PRMM method. For the classical method, NaOH catalyst weights and HSO: methanol molar ratio were obtained to be 5:1 and 0.6 wt%, respectively, for the reaction temperature of 40 °C and reaction time of 60 min, and a yield of 95.05% was acquired. Compared with the classical method, the biodiesel yield of the CSMM and PRMM methods are increased by 0.765% and 1.065%, respectively.

Meanwhile, the different models based on third-degree polynomial equations were generated to reflect the correlation between each optimization parameter and biodiesel yield, with the coefﬁcient of uncertainty (R2) reaching 0.9999 and 1.0000, respectively. All the specified PRMM models showed successfully estimated capability. The prepared hemp seed biodiesel has generally met the EN 14214 standards. In this period of the global food crisis, CSMM and PRMM optimization techniques have proven to be good alternatives in biodiesel production.

References

- Midilli A, Dincer I, Ay M. Green energy strategies for sustainable development. Energy Policy 2006;34(18):3623–3633.

- Mohr SH, Wang J, Ellem G, Ward J, Giurco D. Projection of world fossil fuels by country. Fuel 2015;141:120–135.

- Petroleum B. Full report—Statistical review of world energy 2022. British Petroleum: London, UK, 1–70.

- Srithar K, Balasubramanian KA, Pavendan V, Kumar BA. Experimental investigations on mixing of two biodiesels blended with diesel as alternative fuel for diesel engines. J. King Saud Univ Eng Sci 2017;29(1):50–56.

- Hayashida K, Haji K. Effects of Fuel Properties on Diffusion Combustion and Deposit Accumulation. In: Khan S, editor. Fossil Fuel and the Environment, 1–18, InTech; 2012.

- Singh BR, Singh O. Global Trends of Fossil Fuel Reserves and Climate Change in the 21st Century. In: Khan S, editor. Fossil Fuel and the Environment, 167–192, InTech; 2012.

- Goswami DY, Kreith F. Global Energy Systems. In: Goswami DY, Kreith F, editors. Energy Efficiency and Renewable Energy Handbook, 27–56. Florida: CRC Press; 2016.

- Anani N. Renewable Energy Technologies and Resources. Boston: Artech House; 2020.

- Ahmad M, Khan MA, Zafar M, Sultana S. Practical Handbook on Biodiesel Production and Properties. CRC press; 2012.

- Zahan KA, Kano M. Biodiesel production from palm oil, its by-products, and mill effluent: A review, Energies 2018;11(8):2132.

- Seffati K, Honarvar B, Esmaeili H, Esfandiari N. 2019. Enhanced biodiesel production from chicken fat using CaO/CuFe2O4 nanocatalyst and its combination with diesel to improve fuel properties, Fuel 2019;235:1238–1244.

- Talha NS, Sulaiman S. 2016. Overview of catalysts in biodiesel production, ARPN J Eng Appl Sci 2016;11(1):439–442.

- Bukkarapu KR,  Krishnasamy A. Predicting engine fuel properties of biodiesel and biodiesel-diesel blends using spectroscopy based approach. Fuel Process Technol 2022; 230:107227.

- Atabani AE, et al. A comprehensive review on biodiesel as an alternative energy resource and its characteristics. Renewable Sustainable Energy Rev, 2012;16(4):2070–2093.

- Tran NN, et al. Production of biodiesel from recycled grease trap waste: A review. Ind Eng Chem Res 2021; 60(46):16547–16560.

- Demirbas A, Bafail A, Ahmad W, Sheikh M. Biodiesel production from non-edible plant oils. Energy Explor Exploit 2016;34(2):290–318.

- Deng G, et al. Planting density and fertilization evidently influence the fiber yield of hemp (Cannabis sativa L.). Agron 2019;9(7):368.

- Wirtshafter DE. Ten years of a modern hemp industry. Journal of industrial hemp 2004;9(1):9–14.

- Johnson R. (2014, February). Hemp as an agricultural commodity. Library of Congress Washington DC Congressional Research Service.

- A. Alcheikh, 2015. Advantages and challenges of hemp biodiesel production, Master Thesis. Department of Energy Systems. Faculty of Engineering and Sustainable Development, Gavle University: Gävle, Sweden.

- Strzelczyk M, Lochynska M, Chudy M. Systematics and botanical characteristics of industrial hemp Cannabis sativa L. J Nat Fibers 2022;19(13):5804–5826.

- FAO-Food and Agriculture Organization-Hempseed. https://www.fao.org/faostat/en/#da ta/QCL. Accessed in March 2023.

- Elango RK, et al. Transesterification of castor oil for biodiesel production: Process optimization and characterization. Microchem J 2019;145:1162–1168.

- Abbah EC, Nwandikom GI, Egwuonwu CC, Nwakuba NR. Effect of reaction temperature on the yield of biodiesel from neem seed oil. Am J Energy Sci 2016;3(3):16–20.

- Gupta AR, Jalan AP, Rathod VK. Solar energy as a process intensification tool for the biodiesel production from hempseed oil. Energy Convers Manag 2018;171:126–132.

- Stamenković OS, et al. Optimization of KOH-catalyzed methanolysis of hempseed oil. Energy Convers Manag 2015;103:235–243.

- Yilbasi Z, Yesilyurt MK, Arslan M. The production of methyl ester from industrial grade hemp (Cannabis sativa L.) seed oil: a perspective of Turkey—the optimization study using the Taguchi method. Biomass Convers Biorefin 2021;1–21.

- Rashid U, et al. Biodiesel production from Cannabis sativa oil from Pakistan. Energy Sources A: Recovery Util Environ Eff 2016;38(6):865–875.

- Maindl TI. Introduction to Cubic Spline Interpolation with Examples in Python. CreateSpace Independent Publishing:2018.

- Gupta RK. Numerical methods: Fundamentals and applications. Cambridge University Press:2019.

- Freedman DA. Statistical Models: Theory and Practice. Cambridge University Press:2009.

- Ramírez-Verduzco LF, et al. Predicting cetane number, kinematic viscosity, density and higher heating value of biodiesel from its fatty acid methyl ester composition. Fuel 2012;91(1):102–111.

- Demirbas A. Mathematical relationships derived from biodiesel fuels. Energy Sources A: Recovery Util Environ Eff 2007;30(1):56–69.

- V. Aslan, 2019. Investigation of fuel properties, motor performances and exhaust emissions of biodiesels used by different alcohols and catalysts in production. Doctoral Dissertation, Department of Mechanical Engineering. Faculty of Engineering-Architecture, Yozgat Bozok University: Yozgat, Turkey.

- Sarin A, et al. Effect of blends of Palm-Jatropha-Pongamia biodiesels on cloud point and pour point. Energy 2009;34(11):2016–2021.

- Ramos MJ, et al. Influence of fatty acid composition of raw materials on biodiesel properties. Bioresour Technol 2009;100(1):261–268.

- Agarwal M, Singh K, Chaurasia SP. Prediction of biodiesel properties from fatty acid composition using linear regression and ANN techniques. Indian Chem Eng 2010;52(4):347–361.

- Cao J, et al. Effect of fatty acid and tocopherol on oxidative stability of vegetable oils with limited air. Int J Food Prop 2015;18(4):808–820.

- Dhawane SH, Kumar T, Halder G. Biodiesel synthesis from Hevea brasiliensis oil employing carbon supported heterogeneous catalyst: Optimization by Taguchi method. Renew Energ 2016;89:506–514.

- Miraculas GA, Bose N, Raj RE. Process parameter optimization for biodiesel production from mixed feedstock using empirical model. Sustain Energy Technol Assess 2018;28:54–59.

- Hundie KB, Akuma DA. Optimization of biodiesel production parameters from Prosopis julifera seed using definitive screening design. Heliyon 2022;8(2):e08965.

- Adenuga AA, Idowu OO, Oyekunle JAO. Synthesis of quality biodiesel from Calophyllum inophyllum kernels through reactive extraction method: Optimization of process parameters and characterization of the products. Renew Energ 2020;145:2530–2537.

- Halwe AD, et al. Optimization of the novel hydrodynamic cavitation based waste cooking oil biodiesel production process parameters using integrated L9 Taguchi and RSM approach. Mater Today: Proc 2021;47:5934–5941.

- Sultana S, et al. The production, optimization, and characterization of biodiesel from a novel source: Sinapis alba L. Int J Green Energy 2014;11(3):280–291.

- Almasi S, Najafi G, Ghobadian B, Jalili S. Biodiesel production from sour cherry kernel oil as novel feedstock using potassium hydroxide catalyst: optimization using response surface methodology. Biocatal Agric Biotechnol 2021;35:102089.

- Degfie TA, Mamo TT, Mekonnen YS. Optimized biodiesel production from waste cooking oil (WCO) using calcium oxide (CaO) nano-catalyst. Sci Rep 2019;9(1):18982.

- Pawar S, Hole J, Bankar M, Channapattana S, Srinidhi C. Studies on xanthium strumarium L. seed oil: biodiesel synthesis and process optimization. Mater Today: Proc 2022;66:2169–2177.

- Lakshmana Naik R, et al. Optimized parameters for production of biodiesel from fried oil.  Int Adv Res J Sci Eng Technol 2015;2(6):23.

- Aslan V, Eryilmaz T. Polynomial regression method for optimization of biodiesel production from black mustard (Brassica nigra L.) seed oil using methanol, ethanol, NaOH, and KOH. Energy 2020;209:118386.

- Ahmad M, et al. Physicochemical analysis of hemp oil biodiesel: a promising non edible new source for bioenergy. Energy Sources A: Recovery Util Environ Eff 2011;33(14):1365–1374.

- Yesilyurt MK, Cesur C, Aslan V, Yilbasi Z. The production of biodiesel from safflower (Carthamus tinctorius L.) oil as a potential feedstock and its usage in compression ignition engine: A comprehensive review. Renewable Sustainable Energy Rev 2020;119:109574.

|  | Volkan Aslan A mechanical engineer with a PhD in mechanical engineering, Dr. Aslan is currently an assistant professor and researcher at the Yozgat Bozok University, with experience in biomass, drying, and renewable energy. |
| --- | --- |